| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.851 |  |  | 5.838 |  |  |  | 5.865 |  |  |  |  | 0.46% |  |  |  |  | E |  |  | EX |  |  |  | 5.852 | 5.844 |  | 5.847 | 5.851 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.50 |  |  | 34.13 |  |  |  | 34.74 |  |  |  |  | 0.61 |  |  |  |  | Grading |  |  | VG |  |  |  | 34.74 | 34.70 |  | 34.61 | 34.65 |  |  | 34.24 |  |  | 34.13 |  | 34.25 | 34.67 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.71 |  |  | 41.39 |  |  |  | 42.13 |  |  |  |  | 0.74 |  |  |  |  | Grading |  |  | VG |  |  |  | 41.40 | 41.39 |  | 41.52 | 41.78 |  |  | 41.97 |  |  | 42.13 |  | 41.97 | 41.52 |
| Model |  |  | st1 |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 61.98 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.96 |  |  | 14.67 |  |  |  | 15.23 |  |  |  |  | 0.56 |  |  |  |  | E |  |  | EX |  |  |  | 14.82 | 15.00 |  | 15.21 | 15.23 |  |  | 14.99 |  |  | 14.93 |  | 14.67 | 14.87 |
| Report date |  |  | 10.12.2007 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 44.40 |  |  | 44.05 |  |  |  | 44.73 |  |  |  |  | 0.68 |  |  |  |  | N/A |  |  | EX |  |  |  | 44.68 | 44.27 |  | 44.06 | 44.05 |  |  | 44.19 |  |  | 44.62 |  | 44.73 | 44.61 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 56.32 |  |  | 56.09 |  |  |  | 56.48 |  |  |  |  | 0.40 |  |  |  |  | Grading |  |  | EX |  |  |  | 56.48 | 56.09 |  | 56.30 | 56.42 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.74, 0.7451 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.33 |  |  | 0.21 |  |  |  | 0.40 |  |  |  |  | 0.19 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.851 (5.838-5.865) x 3.626 /0.004 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 2.61 |  |  | 2.42 |  |  |  | 2.78 |  |  |  |  | 0.36 |  |  |  |  | E |  |  | EX |  |  |  | 2.48 | 2.72 |  | 2.71 | 2.71 |  |  | 2.78 |  |  | 2.42 |  | 2.58 | 2.49 |
| Spread |  |  | 0.00 ct, 0.24% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 2.98 |  |  | 2.70 |  |  |  | 3.14 |  |  |  |  | 0.43 |  |  |  |  |  |  |  | EX |  |  |  | 2.93 | 2.81 |  | 3.08 | 3.12 |  |  | 2.70 |  |  | 3.14 |  | 2.90 | 3.13 |
| AGS Spread |  |  | -0.00 ct, -0.07% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.17 |  |  | 0.96 |  |  |  | 1.39 |  |  |  |  | 0.43 |  |  |  |  | E |  |  | EX |  |  |  | 1.29 | 1.23 |  | 1.14 | 1.21 |  |  | 1.10 |  |  | 1.17 |  | 1.22 | 1.11 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.22 | 0.96 |  | 0.96 | 1.25 |  |  | 1.39 |  |  | 1.04 |  | 1.26 | 1.22 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 56.02: |  |  | 54.07: |  |  |  | 57.10: |  |  |  |  | 3.03 |  |  |  |  | E |  |  | VG |  |  |  | 56.64: | 56.75: |  | 54.07: | 54.49: |  |  | 55.70: |  |  | 56.92: |  | 56.49: | 57.10: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 43.98 |  |  | 45.93 |  |  |  | 42.90 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 43.36 | 43.25 |  | 45.93 | 45.51 |  |  | 44.30 |  |  | 43.08 |  | 43.51 | 42.90 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 22.93 |  |  | 22.76 |  |  |  | 23.04 |  |  |  |  | 0.28 |  |  |  |  |  |  |  | EX |  |  |  | 23.04 | 22.93 |  | 23.04 | 22.76 |  |  | 22.87 |  |  | 22.87 |  | 22.99 | 22.96 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 41.11 |  |  | 40.18 |  |  |  | 42.14 |  |  |  |  | 1.95 |  |  |  |  |  |  |  | VG |  |  |  | 41.49 | 41.64 |  | 42.14 | 41.77 |  |  | 41.10 |  |  | 40.92 |  | 41.20 | 40.84 |
| 5.851 | 3.626 | 0.876 | 2.598 | 3.295 |  | 0.019 | 0.153 | 0.174 | 0.069 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.21 | 40.94 |  | 40.18 | 40.87 |  |  | 40.68 |  |  | 40.82 |  | 40.88 | 41.14 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 80.27 |  |  | 78.66 |  |  |  | 81.28 |  |  |  |  | 2.62 |  |  |  |  | E |  |  | EX |  |  |  | 78.66 | 79.71 |  | 79.38 | 78.98 |  |  | 80.01 |  |  | 80.41 |  | 79.66 | 81.03 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 81.14 | 80.73 |  | 81.28 | 81.17 |  |  | 80.96 |  |  | 80.62 |  | 80.61 | 80.02 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.72 |  |  | 42.22 |  |  |  | 43.27 |  |  |  |  | 1.05 |  |  |  |  |  |  |  | VG |  |  |  | 42.22 | 42.33 |  | 42.37 | 42.53 |  |  | 42.46 |  |  | 42.70 |  | 42.94 | 43.04 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 43.19 | 43.27 |  | 43.09 | 43.05 |  |  | 42.82 |  |  | 42.71 |  | 42.42 | 42.35 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.84 |  |  | 0.27 |  |  |  | 1.31 |  |  |  |  | 1.04 |  |  |  |  |  |  |  | VG |  |  |  | 0.98 | 1.21 |  | 0.62 | 1.31 |  |  | 1.03 |  |  | 0.27 |  | 0.97 | 0.34 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.876 |  |  | 0.858 |  |  |  | 0.891 |  |  |  |  | 0.033 |  |  |  |  | E |  |  | EX |  |  |  | 0.867 | 0.877 |  | 0.890 | 0.891 |  |  | 0.877 |  |  | 0.874 |  | 0.858 | 0.870 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.598 |  |  | 2.577 |  |  |  | 2.617 |  |  |  |  | 0.040 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.614 | 2.590 |  | 2.578 | 2.577 |  |  | 2.586 |  |  | 2.611 |  | 2.617 | 2.610 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.295 |  |  | 3.282 |  |  |  | 3.305 |  |  |  |  | 0.023 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.305 | 3.282 |  | 3.294 | 3.301 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.019 |  |  | 0.012 |  |  |  | 0.023 |  |  |  |  | 0.011 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.153 |  |  | 0.142 |  |  |  | 0.163 |  |  |  |  | 0.021 |  |  |  |  | E |  |  | EX |  |  |  | 0.145 | 0.159 |  | 0.159 | 0.158 |  |  | 0.163 |  |  | 0.142 |  | 0.151 | 0.146 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.174 |  |  | 0.158 |  |  |  | 0.184 |  |  |  |  | 0.025 |  |  |  |  |  |  |  | EX |  |  |  | 0.171 | 0.165 |  | 0.180 | 0.182 |  |  | 0.158 |  |  | 0.184 |  | 0.170 | 0.183 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.069 |  |  | 0.056 |  |  |  | 0.081 |  |  |  |  | 0.025 |  |  |  |  | E |  |  | EX |  |  |  | 0.075 | 0.072 |  | 0.067 | 0.071 |  |  | 0.064 |  |  | 0.069 |  | 0.072 | 0.065 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.071 | 0.056 |  | 0.056 | 0.073 |  |  | 0.081 |  |  | 0.061 |  | 0.074 | 0.071 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.50 |  |  | 34.42 |  |  |  | 34.66 |  |  |  |  | 0.24 |  |  |  |  |  |  |  |  |  |  |  | 34.49 | 34.42 |  | 34.43 | 34.66 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.71 |  |  | 41.65 |  |  |  | 41.76 |  |  |  |  | 0.11 |  |  |  |  |  |  |  |  |  |  |  | 41.68 | 41.76 |  | 41.74 | 41.65 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 12.35 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 9.45 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.004 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | -2.43 |  |  |  |  | -0.06 | -0.28 |  |  |  | -0.31 |  |  | -1.19 | 0.06 |  | -0.14 |  |  | Crown, ° |  | -1.13 |  |  |  | Painting |  |  | EX |  | -2.21 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | -0.98 |  |  | -1.22 |  |  |  |  | -0.69 | -1.59 |  |  |  | -1.34 |  |  | -0.92 | -0.92 |  | -0.48 |  |  | Crown, notch. |  | 0.3, Small |  |  |  |  |  |  |  |  | 0.6 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.77 |  |  | -1.36 |  |  |  |  | -0.11 | -0.80 |  |  |  | -0.84 |  |  | -1.35 | -0.30 |  | -1.16 |  |  | Pavilion, ° |  | -0.51 |  |  |  | Painting |  |  | EX |  | -2.81 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.02 |  |  | -0.75 |  |  |  |  | -2.16 | -1.57 |  |  |  | -1.37 |  |  | -1.65 | -2.21 |  | -1.67 |  |  | Pavilion, notch. |  | 0.1, Very small |  |  |  |  |  |  |  |  | 0.7 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | -2.81 |  |  | -1.49 |  |  |  |  | -0.01 | 0.37 |  |  |  | -2.07 |  |  | -0.54 | -0.34 |  | -0.02 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.35 |  |  | -0.37 |  |  |  |  | -0.26 | 0.13 |  |  |  | -1.54 |  |  | 1.23 | -1.37 |  | -0.36 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | V |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.75 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.044 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.34 ± 0.19, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.020 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.99 ± 0.23, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.058 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.21 %, 0.012 mm |  |  |  |  |  |