| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.852 |  |  | 5.842 |  |  |  | 5.861 |  |  |  |  | 0.32% |  |  |  |  | E |  |  | EX |  |  |  | 5.856 | 5.858 |  | 5.853 | 5.855 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.52 |  |  | 34.40 |  |  |  | 34.65 |  |  |  |  | 0.25 |  |  |  |  | Grading |  |  | EX |  |  |  | 34.65 | 34.61 |  | 34.43 | 34.40 |  |  | 34.42 |  |  | 34.49 |  | 34.53 | 34.60 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 42.22 |  |  | 42.06 |  |  |  | 42.34 |  |  |  |  | 0.28 |  |  |  |  | Grading |  |  | EX |  |  |  | 42.06 | 42.20 |  | 42.34 | 42.34 |  |  | 42.25 |  |  | 42.23 |  | 42.22 | 42.09 |
| Model |  |  | Simple |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 62.73 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.70 |  |  | 14.52 |  |  |  | 14.91 |  |  |  |  | 0.38 |  |  |  |  | E |  |  | EX |  |  |  | 14.91 | 14.79 |  | 14.60 | 14.56 |  |  | 14.52 |  |  | 14.64 |  | 14.73 | 14.84 |
| Report date |  |  | 17.04.2008 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 45.26 |  |  | 45.04 |  |  |  | 45.45 |  |  |  |  | 0.41 |  |  |  |  | N/A |  |  | EX |  |  |  | 45.04 | 45.26 |  | 45.40 | 45.45 |  |  | 45.37 |  |  | 45.29 |  | 45.21 | 45.06 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.38 |  |  | 57.35 |  |  |  | 57.43 |  |  |  |  | 0.08 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.38 | 57.43 |  | 57.35 | 57.35 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.75, 0.7555 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.31 |  |  | 0.22 |  |  |  | 0.38 |  |  |  |  | 0.16 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.852 (5.842-5.861) x 3.671 /0.001 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 2.76 |  |  | 2.68 |  |  |  | 2.83 |  |  |  |  | 0.15 |  |  |  |  | E |  |  | EX |  |  |  | 2.79 | 2.68 |  | 2.73 | 2.72 |  |  | 2.82 |  |  | 2.79 |  | 2.76 | 2.83 |
| Spread |  |  | -0.01 ct, -1.02% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 2.81 |  |  | 2.72 |  |  |  | 2.89 |  |  |  |  | 0.18 |  |  |  |  |  |  |  | EX |  |  |  | 2.77 | 2.79 |  | 2.78 | 2.89 |  |  | 2.87 |  |  | 2.72 |  | 2.83 | 2.82 |
| AGS Spread |  |  | N/A ct, N/A% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.17 |  |  | 1.04 |  |  |  | 1.28 |  |  |  |  | 0.25 |  |  |  |  | E |  |  | EX |  |  |  | 1.11 | 1.04 |  | 1.10 | 1.19 |  |  | 1.19 |  |  | 1.04 |  | 1.12 | 1.22 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.28 | 1.27 |  | 1.26 | 1.12 |  |  | 1.18 |  |  | 1.09 |  | 1.22 | 1.23 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 55.37: |  |  | 54.68: |  |  |  | 55.92: |  |  |  |  | 1.24 |  |  |  |  | E |  |  | EX |  |  |  | 55.73: | 54.68: |  | 55.10: | 55.68: |  |  | 55.92: |  |  | 55.16: |  | 55.42: | 55.30: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 44.63 |  |  | 45.32 |  |  |  | 44.08 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 44.27 | 45.32 |  | 44.90 | 44.32 |  |  | 44.08 |  |  | 44.84 |  | 44.58 | 44.70 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 22.61 |  |  | 22.32 |  |  |  | 22.81 |  |  |  |  | 0.49 |  |  |  |  |  |  |  | EX |  |  |  | 22.81 | 22.63 |  | 22.32 | 22.55 |  |  | 22.65 |  |  | 22.44 |  | 22.65 | 22.80 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 41.99 |  |  | 41.63 |  |  |  | 42.32 |  |  |  |  | 0.69 |  |  |  |  |  |  |  | EX |  |  |  | 42.04 | 42.32 |  | 41.82 | 41.63 |  |  | 41.88 |  |  | 41.87 |  | 42.08 | 41.99 |
| 5.852 | 3.671 | 0.860 | 2.649 | 3.358 |  | 0.018 | 0.162 | 0.164 | 0.068 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.87 | 41.83 |  | 41.98 | 42.30 |  |  | 41.76 |  |  | 42.13 |  | 42.17 | 42.15 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 79.78 |  |  | 79.19 |  |  |  | 80.75 |  |  |  |  | 1.55 |  |  |  |  | E |  |  | EX |  |  |  | 79.36 | 80.14 |  | 80.75 | 79.89 |  |  | 79.43 |  |  | 79.79 |  | 80.05 | 79.54 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 79.68 | 79.19 |  | 79.42 | 79.50 |  |  | 79.93 |  |  | 79.58 |  | 80.15 | 80.05 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 43.32 |  |  | 43.12 |  |  |  | 43.46 |  |  |  |  | 0.34 |  |  |  |  |  |  |  | EX |  |  |  | 43.20 | 43.28 |  | 43.32 | 43.40 |  |  | 43.44 |  |  | 43.46 |  | 43.39 | 43.35 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 43.32 | 43.32 |  | 43.34 | 43.39 |  |  | 43.31 |  |  | 43.29 |  | 43.12 | 43.12 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.47 |  |  | 0.10 |  |  |  | 1.07 |  |  |  |  | 0.98 |  |  |  |  |  |  |  | EX |  |  |  | 0.33 | 0.36 |  | 0.23 | 0.10 |  |  | 0.44 |  |  | 1.07 |  | 0.75 | 0.49 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.860 |  |  | 0.850 |  |  |  | 0.872 |  |  |  |  | 0.022 |  |  |  |  | E |  |  | EX |  |  |  | 0.872 | 0.866 |  | 0.854 | 0.852 |  |  | 0.850 |  |  | 0.857 |  | 0.862 | 0.868 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.649 |  |  | 2.636 |  |  |  | 2.660 |  |  |  |  | 0.024 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.636 | 2.648 |  | 2.657 | 2.660 |  |  | 2.655 |  |  | 2.651 |  | 2.646 | 2.637 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.358 |  |  | 3.356 |  |  |  | 3.361 |  |  |  |  | 0.005 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.358 | 3.361 |  | 3.356 | 3.356 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.018 |  |  | 0.013 |  |  |  | 0.022 |  |  |  |  | 0.009 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.162 |  |  | 0.157 |  |  |  | 0.166 |  |  |  |  | 0.009 |  |  |  |  | E |  |  | EX |  |  |  | 0.163 | 0.157 |  | 0.160 | 0.159 |  |  | 0.165 |  |  | 0.163 |  | 0.161 | 0.166 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.164 |  |  | 0.159 |  |  |  | 0.169 |  |  |  |  | 0.010 |  |  |  |  |  |  |  | EX |  |  |  | 0.162 | 0.163 |  | 0.163 | 0.169 |  |  | 0.168 |  |  | 0.159 |  | 0.166 | 0.165 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.068 |  |  | 0.061 |  |  |  | 0.075 |  |  |  |  | 0.014 |  |  |  |  | E |  |  | EX |  |  |  | 0.065 | 0.061 |  | 0.064 | 0.070 |  |  | 0.070 |  |  | 0.061 |  | 0.066 | 0.071 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.075 | 0.074 |  | 0.074 | 0.065 |  |  | 0.069 |  |  | 0.064 |  | 0.072 | 0.072 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.52 |  |  | 34.48 |  |  |  | 34.55 |  |  |  |  | 0.07 |  |  |  |  |  |  |  |  |  |  |  | 34.53 | 34.55 |  | 34.48 | 34.50 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 42.22 |  |  | 42.16 |  |  |  | 42.28 |  |  |  |  | 0.12 |  |  |  |  |  |  |  |  |  |  |  | 42.16 | 42.22 |  | 42.28 | 42.22 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 13.85 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 9.79 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.001 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | 0.52 |  |  |  |  | 0.21 | 0.21 |  |  |  | 0.09 |  |  | -0.47 | -0.18 |  | -0.02 |  |  | Crown, ° |  | -0.16 |  |  |  |  |  |  | EX |  | -0.62 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.33 |  |  | 0.16 |  |  |  |  | -0.01 | 0.31 |  |  |  | 0.53 |  |  | 0.60 | 0.56 |  | 0.47 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.2 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.49 |  |  | 0.25 |  |  |  |  | -0.47 | -0.62 |  |  |  | -0.06 |  |  | -0.33 | 0.12 |  | -0.04 |  |  | Pavilion, ° |  | -0.02 |  |  |  |  |  |  | EX |  | 0.34 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.37 |  |  | -0.02 |  |  |  |  | -0.31 | 0.44 |  |  |  | -0.50 |  |  | -0.12 | -0.01 |  | -0.02 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.1 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | 0.14 |  |  | 0.25 |  |  |  |  | -0.27 | -0.29 |  |  |  | 0.03 |  |  | -0.22 | -0.05 |  | -0.15 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.19 |  |  | -0.28 |  |  |  |  | 0.33 | 0.21 |  |  |  | 0.06 |  |  | 0.34 | -0.09 |  | -0.11 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | V |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.03 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.002 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.19 ± 0.19, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.011 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.16 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.009 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.15 %, 0.009 mm |  |  |  |  |  |