| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.763 |  |  | 5.755 |  |  |  | 5.769 |  |  |  |  | 0.24% |  |  |  |  | E |  |  | EX |  |  |  | 5.765 | 5.763 |  | 5.763 | 5.765 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 36.32 |  |  | 36.27 |  |  |  | 36.40 |  |  |  |  | 0.13 |  |  |  |  | Grading |  |  | EX |  |  |  | 36.29 | 36.33 |  | 36.34 | 36.31 |  |  | 36.33 |  |  | 36.27 |  | 36.40 | 36.28 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.18 |  |  | 41.11 |  |  |  | 41.26 |  |  |  |  | 0.15 |  |  |  |  | Grading |  |  | EX |  |  |  | 41.15 | 41.19 |  | 41.26 | 41.18 |  |  | 41.21 |  |  | 41.23 |  | 41.13 | 41.11 |
| Model |  |  | Simple |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 62.29 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 15.74 |  |  | 15.62 |  |  |  | 15.80 |  |  |  |  | 0.18 |  |  |  |  | E |  |  | EX |  |  |  | 15.62 | 15.67 |  | 15.74 | 15.76 |  |  | 15.79 |  |  | 15.77 |  | 15.78 | 15.80 |
| Report date |  |  | 18.04.2008 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 43.58 |  |  | 43.44 |  |  |  | 43.70 |  |  |  |  | 0.25 |  |  |  |  | N/A |  |  | EX |  |  |  | 43.68 | 43.70 |  | 43.65 | 43.44 |  |  | 43.48 |  |  | 43.61 |  | 43.52 | 43.55 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.26 |  |  | 57.18 |  |  |  | 57.34 |  |  |  |  | 0.17 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.34 | 57.24 |  | 57.27 | 57.18 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.73, 0.7291 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.41 |  |  | 0.37 |  |  |  | 0.44 |  |  |  |  | 0.07 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.763 (5.755-5.769) x 3.590 /0.002 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 2.96 |  |  | 2.89 |  |  |  | 3.09 |  |  |  |  | 0.20 |  |  |  |  | E |  |  | EX |  |  |  | 2.99 | 2.91 |  | 2.91 | 3.09 |  |  | 3.00 |  |  | 2.89 |  | 2.96 | 2.95 |
| Spread |  |  | -0.02 ct, -2.96% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 2.97 |  |  | 2.85 |  |  |  | 3.27 |  |  |  |  | 0.42 |  |  |  |  |  |  |  | EX |  |  |  | 3.03 | 2.99 |  | 3.27 | 2.94 |  |  | 2.85 |  |  | 2.91 |  | 2.89 | 2.85 |
| AGS Spread |  |  | N/A ct, N/A% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.23 |  |  | 1.09 |  |  |  | 1.46 |  |  |  |  | 0.36 |  |  |  |  | E |  |  | EX |  |  |  | 1.22 | 1.18 |  | 1.24 | 1.24 |  |  | 1.38 |  |  | 1.46 |  | 1.27 | 1.26 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.23 | 1.09 |  | 1.24 | 1.23 |  |  | 1.23 |  |  | 1.14 |  | 1.17 | 1.16 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 54.74: |  |  | 54.38: |  |  |  | 55.16: |  |  |  |  | 0.78 |  |  |  |  | E |  |  | EX |  |  |  | 54.44: | 54.89: |  | 54.92: | 54.78: |  |  | 55.16: |  |  | 54.38: |  | 54.41: | 54.92: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 45.26 |  |  | 45.62 |  |  |  | 44.84 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 45.56 | 45.11 |  | 45.08 | 45.22 |  |  | 44.84 |  |  | 45.62 |  | 45.59 | 45.08 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 24.02 |  |  | 23.86 |  |  |  | 24.12 |  |  |  |  | 0.26 |  |  |  |  |  |  |  | EX |  |  |  | 23.86 | 24.08 |  | 24.10 | 24.03 |  |  | 24.00 |  |  | 23.98 |  | 24.12 | 24.00 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 43.82 |  |  | 43.35 |  |  |  | 44.42 |  |  |  |  | 1.07 |  |  |  |  |  |  |  | VG |  |  |  | 43.45 | 43.65 |  | 43.98 | 44.16 |  |  | 43.35 |  |  | 43.39 |  | 44.14 | 44.42 |
| 5.763 | 3.590 | 0.907 | 2.511 | 3.300 |  | 0.024 | 0.171 | 0.171 | 0.071 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 43.81 | 44.17 |  | 43.62 | 43.59 |  |  | 43.56 |  |  | 43.93 |  | 43.76 | 44.14 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 79.78 |  |  | 78.94 |  |  |  | 80.47 |  |  |  |  | 1.53 |  |  |  |  | E |  |  | EX |  |  |  | 80.47 | 80.10 |  | 79.81 | 79.63 |  |  | 79.88 |  |  | 79.85 |  | 79.42 | 78.94 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 79.90 | 79.41 |  | 79.66 | 80.33 |  |  | 80.20 |  |  | 79.91 |  | 79.21 | 79.82 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.29 |  |  | 42.18 |  |  |  | 42.37 |  |  |  |  | 0.20 |  |  |  |  |  |  |  | EX |  |  |  | 42.26 | 42.31 |  | 42.33 | 42.37 |  |  | 42.34 |  |  | 42.31 |  | 42.33 | 42.35 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.33 | 42.37 |  | 42.34 | 42.25 |  |  | 42.18 |  |  | 42.20 |  | 42.19 | 42.24 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.36 |  |  | 0.09 |  |  |  | 0.73 |  |  |  |  | 0.63 |  |  |  |  |  |  |  | EX |  |  |  | 0.38 | 0.73 |  | 0.30 | 0.35 |  |  | 0.09 |  |  | 0.46 |  | 0.25 | 0.34 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.907 |  |  | 0.900 |  |  |  | 0.911 |  |  |  |  | 0.010 |  |  |  |  | E |  |  | EX |  |  |  | 0.900 | 0.903 |  | 0.907 | 0.908 |  |  | 0.910 |  |  | 0.909 |  | 0.910 | 0.911 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.511 |  |  | 2.504 |  |  |  | 2.518 |  |  |  |  | 0.015 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.517 | 2.518 |  | 2.515 | 2.504 |  |  | 2.506 |  |  | 2.513 |  | 2.508 | 2.510 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.300 |  |  | 3.295 |  |  |  | 3.305 |  |  |  |  | 0.010 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.305 | 3.299 |  | 3.300 | 3.295 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.024 |  |  | 0.021 |  |  |  | 0.025 |  |  |  |  | 0.004 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.171 |  |  | 0.166 |  |  |  | 0.178 |  |  |  |  | 0.012 |  |  |  |  | E |  |  | EX |  |  |  | 0.173 | 0.168 |  | 0.167 | 0.178 |  |  | 0.173 |  |  | 0.166 |  | 0.170 | 0.170 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.171 |  |  | 0.164 |  |  |  | 0.188 |  |  |  |  | 0.024 |  |  |  |  |  |  |  | EX |  |  |  | 0.175 | 0.172 |  | 0.188 | 0.169 |  |  | 0.164 |  |  | 0.168 |  | 0.167 | 0.164 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.071 |  |  | 0.063 |  |  |  | 0.084 |  |  |  |  | 0.021 |  |  |  |  | E |  |  | EX |  |  |  | 0.070 | 0.068 |  | 0.071 | 0.072 |  |  | 0.080 |  |  | 0.084 |  | 0.073 | 0.072 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.071 | 0.063 |  | 0.071 | 0.071 |  |  | 0.071 |  |  | 0.066 |  | 0.067 | 0.067 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 36.32 |  |  | 36.29 |  |  |  | 36.37 |  |  |  |  | 0.07 |  |  |  |  |  |  |  |  |  |  |  | 36.31 | 36.30 |  | 36.37 | 36.29 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.18 |  |  | 41.15 |  |  |  | 41.21 |  |  |  |  | 0.06 |  |  |  |  |  |  |  |  |  |  |  | 41.18 | 41.21 |  | 41.19 | 41.15 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 9.55 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 7.06 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.002 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | -0.13 |  |  |  |  | -0.05 | -0.05 |  |  |  | 0.04 |  |  | -0.08 | 0.09 |  | 0.01 |  |  | Crown, ° |  | -0.09 |  |  |  |  |  |  | EX |  | 0.79 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.38 |  |  | 0.60 |  |  |  |  | 0.25 | 0.29 |  |  |  | 0.13 |  |  | 0.38 | 0.34 |  | 0.35 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.2 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.70 |  |  | -0.19 |  |  |  |  | 0.07 | -0.04 |  |  |  | -0.47 |  |  | -0.66 | 0.36 |  | 0.79 |  |  | Pavilion, ° |  | 0.12 |  |  |  |  |  |  | EX |  | 0.48 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.35 |  |  | 0.32 |  |  |  |  | -0.28 | -0.43 |  |  |  | -0.37 |  |  | 0.31 | -0.47 |  | 0.70 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.1 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | 0.08 |  |  | -0.03 |  |  |  |  | 0.30 | -0.17 |  |  |  | 0.07 |  |  | 0.30 | 0.15 |  | 0.48 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.09 |  |  | -0.04 |  |  |  |  | 0.42 | 0.25 |  |  |  | -0.05 |  |  | 0.27 | -0.17 |  | -0.08 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.20 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.012 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.11 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.006 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.19 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.011 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.11 %, 0.006 mm |  |  |  |  |  |