| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.841 |  |  | 5.835 |  |  |  | 5.845 |  |  |  |  | 0.16% |  |  |  |  | E |  |  | EX |  |  |  | 5.842 | 5.841 |  | 5.842 | 5.842 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.03 |  |  | 33.89 |  |  |  | 34.18 |  |  |  |  | 0.29 |  |  |  |  | Grading |  |  | EX |  |  |  | 34.18 | 34.07 |  | 33.89 | 33.98 |  |  | 33.96 |  |  | 33.99 |  | 34.06 | 34.09 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.98 |  |  | 40.79 |  |  |  | 41.12 |  |  |  |  | 0.33 |  |  |  |  | Grading |  |  | EX |  |  |  | 40.79 | 40.93 |  | 41.12 | 41.06 |  |  | 41.11 |  |  | 40.99 |  | 40.94 | 40.92 |
| Model |  |  | Simple |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 60.80 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.42 |  |  | 14.32 |  |  |  | 14.53 |  |  |  |  | 0.21 |  |  |  |  | E |  |  | EX |  |  |  | 14.53 | 14.52 |  | 14.36 | 14.32 |  |  | 14.35 |  |  | 14.33 |  | 14.44 | 14.51 |
| Report date |  |  | 10.03.2008 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 43.30 |  |  | 43.09 |  |  |  | 43.43 |  |  |  |  | 0.34 |  |  |  |  | N/A |  |  | EX |  |  |  | 43.09 | 43.26 |  | 43.43 | 43.32 |  |  | 43.43 |  |  | 43.26 |  | 43.29 | 43.29 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.38 |  |  | 57.35 |  |  |  | 57.41 |  |  |  |  | 0.06 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.40 | 57.37 |  | 57.35 | 57.41 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.73, 0.7370 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.39 |  |  | 0.36 |  |  |  | 0.41 |  |  |  |  | 0.05 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.841 (5.835-5.845) x 3.551 /0.001 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 3.07 |  |  | 2.95 |  |  |  | 3.21 |  |  |  |  | 0.26 |  |  |  |  | E |  |  | EX |  |  |  | 3.21 | 3.02 |  | 3.00 | 3.16 |  |  | 3.00 |  |  | 3.20 |  | 3.07 | 2.95 |
| Spread |  |  | 0.01 ct, 1.11% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 3.09 |  |  | 3.02 |  |  |  | 3.23 |  |  |  |  | 0.21 |  |  |  |  |  |  |  | EX |  |  |  | 3.04 | 3.02 |  | 3.23 | 3.04 |  |  | 3.18 |  |  | 3.11 |  | 3.04 | 3.03 |
| AGS Spread |  |  | N/A ct, N/A% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.45 |  |  | 1.28 |  |  |  | 1.65 |  |  |  |  | 0.38 |  |  |  |  | E |  |  | EX |  |  |  | 1.63 | 1.43 |  | 1.31 | 1.28 |  |  | 1.48 |  |  | 1.65 |  | 1.47 | 1.39 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.43 | 1.58 |  | 1.63 | 1.38 |  |  | 1.34 |  |  | 1.31 |  | 1.39 | 1.49 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 55.08: |  |  | 54.03: |  |  |  | 56.31: |  |  |  |  | 2.28 |  |  |  |  | E |  |  | VG |  |  |  | 54.03: | 56.06: |  | 54.66: | 54.04: |  |  | 55.38: |  |  | 55.52: |  | 56.31: | 54.66: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 44.92 |  |  | 45.97 |  |  |  | 43.69 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 45.97 | 43.94 |  | 45.34 | 45.96 |  |  | 44.62 |  |  | 44.48 |  | 43.69 | 45.34 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 22.14 |  |  | 21.87 |  |  |  | 22.35 |  |  |  |  | 0.48 |  |  |  |  |  |  |  | EX |  |  |  | 22.16 | 22.20 |  | 22.02 | 21.87 |  |  | 22.33 |  |  | 22.35 |  | 22.21 | 22.00 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 41.57 |  |  | 41.26 |  |  |  | 42.00 |  |  |  |  | 0.74 |  |  |  |  |  |  |  | EX |  |  |  | 41.50 | 41.71 |  | 41.42 | 41.48 |  |  | 41.43 |  |  | 41.36 |  | 41.32 | 41.80 |
| 5.841 | 3.551 | 0.842 | 2.529 | 3.352 |  | 0.023 | 0.180 | 0.180 | 0.085 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.39 | 41.46 |  | 41.26 | 41.83 |  |  | 41.79 |  |  | 42.00 |  | 41.82 | 41.61 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 79.70 |  |  | 78.90 |  |  |  | 80.40 |  |  |  |  | 1.50 |  |  |  |  | E |  |  | EX |  |  |  | 78.99 | 79.73 |  | 79.76 | 80.05 |  |  | 80.08 |  |  | 80.20 |  | 79.29 | 79.85 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 78.90 | 79.08 |  | 80.20 | 80.40 |  |  | 79.87 |  |  | 80.22 |  | 79.55 | 79.01 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.07 |  |  | 41.86 |  |  |  | 42.22 |  |  |  |  | 0.36 |  |  |  |  |  |  |  | EX |  |  |  | 41.86 | 41.96 |  | 42.11 | 42.20 |  |  | 42.12 |  |  | 42.08 |  | 42.16 | 42.19 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.22 | 42.11 |  | 42.00 | 42.04 |  |  | 42.07 |  |  | 42.07 |  | 42.01 | 41.90 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.40 |  |  | 0.15 |  |  |  | 0.75 |  |  |  |  | 0.60 |  |  |  |  |  |  |  | EX |  |  |  | 0.33 | 0.19 |  | 0.35 | 0.15 |  |  | 0.41 |  |  | 0.75 |  | 0.55 | 0.43 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.842 |  |  | 0.837 |  |  |  | 0.849 |  |  |  |  | 0.012 |  |  |  |  | E |  |  | EX |  |  |  | 0.849 | 0.848 |  | 0.839 | 0.837 |  |  | 0.838 |  |  | 0.837 |  | 0.843 | 0.848 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.529 |  |  | 2.517 |  |  |  | 2.537 |  |  |  |  | 0.020 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.517 | 2.527 |  | 2.537 | 2.530 |  |  | 2.537 |  |  | 2.527 |  | 2.529 | 2.529 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.352 |  |  | 3.350 |  |  |  | 3.353 |  |  |  |  | 0.003 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.353 | 3.351 |  | 3.350 | 3.353 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.023 |  |  | 0.021 |  |  |  | 0.024 |  |  |  |  | 0.003 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.180 |  |  | 0.172 |  |  |  | 0.187 |  |  |  |  | 0.015 |  |  |  |  | E |  |  | EX |  |  |  | 0.187 | 0.176 |  | 0.175 | 0.184 |  |  | 0.175 |  |  | 0.187 |  | 0.179 | 0.172 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.180 |  |  | 0.177 |  |  |  | 0.189 |  |  |  |  | 0.012 |  |  |  |  |  |  |  | EX |  |  |  | 0.178 | 0.177 |  | 0.189 | 0.178 |  |  | 0.186 |  |  | 0.181 |  | 0.178 | 0.177 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.085 |  |  | 0.075 |  |  |  | 0.097 |  |  |  |  | 0.022 |  |  |  |  | E |  |  | EX |  |  |  | 0.095 | 0.084 |  | 0.077 | 0.075 |  |  | 0.086 |  |  | 0.097 |  | 0.086 | 0.081 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.083 | 0.092 |  | 0.095 | 0.081 |  |  | 0.078 |  |  | 0.076 |  | 0.081 | 0.087 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.03 |  |  | 33.97 |  |  |  | 34.07 |  |  |  |  | 0.10 |  |  |  |  |  |  |  |  |  |  |  | 34.07 | 34.03 |  | 33.97 | 34.03 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.98 |  |  | 40.95 |  |  |  | 41.03 |  |  |  |  | 0.08 |  |  |  |  |  |  |  |  |  |  |  | 40.95 | 40.96 |  | 41.03 | 40.99 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 8.75 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 12.36 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.001 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | -0.02 |  |  |  |  | 0.33 | 0.12 |  |  |  | 0.10 |  |  | -0.48 | -0.64 |  | -0.10 |  |  | Crown, ° |  | -0.02 |  |  |  |  |  |  | EX |  | 0.85 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.33 |  |  | 0.17 |  |  |  |  | -0.03 | 0.27 |  |  |  | 0.51 |  |  | 0.27 | -0.09 |  | 0.34 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.2 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.08 |  |  | 0.65 |  |  |  |  | -0.61 | -0.28 |  |  |  | 0.32 |  |  | -0.08 | -0.27 |  | 0.85 |  |  | Pavilion, ° |  | -0.03 |  |  |  |  |  |  | EX |  | -0.41 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.67 |  |  | -0.15 |  |  |  |  | -0.51 | 0.32 |  |  |  | -0.20 |  |  | 0.02 | 0.32 |  | 0.03 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.1 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | 0.03 |  |  | -0.10 |  |  |  |  | 0.24 | -0.09 |  |  |  | -0.32 |  |  | -0.08 | -0.22 |  | 0.18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.41 |  |  | -0.30 |  |  |  |  | -0.05 | -0.22 |  |  |  | 0.36 |  |  | 0.25 | 0.04 |  | 0.16 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.11 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.007 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.14 ± 0.19, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.008 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.07 ± 0.23, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.004 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.13 %, 0.008 mm |  |  |  |  |  |