| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.841 |  |  | 5.835 |  |  |  | 5.846 |  |  |  |  | 0.18% |  |  |  |  | E |  |  | EX |  |  |  | 5.840 | 5.845 |  | 5.840 | 5.842 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 33.53 |  |  | 33.36 |  |  |  | 33.68 |  |  |  |  | 0.32 |  |  |  |  | Grading |  |  | EX |  |  |  | 33.53 | 33.68 |  | 33.66 | 33.62 |  |  | 33.60 |  |  | 33.36 |  | 33.38 | 33.40 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.98 |  |  | 40.73 |  |  |  | 41.21 |  |  |  |  | 0.48 |  |  |  |  | Grading |  |  | EX |  |  |  | 40.93 | 40.73 |  | 40.77 | 40.94 |  |  | 40.99 |  |  | 41.17 |  | 41.21 | 41.06 |
| Model |  |  | Simple |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 60.73 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.26 |  |  | 14.06 |  |  |  | 14.41 |  |  |  |  | 0.35 |  |  |  |  | E |  |  | EX |  |  |  | 14.40 | 14.41 |  | 14.37 | 14.29 |  |  | 14.20 |  |  | 14.06 |  | 14.07 | 14.25 |
| Report date |  |  | 10.03.2008 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 43.28 |  |  | 43.14 |  |  |  | 43.41 |  |  |  |  | 0.27 |  |  |  |  | N/A |  |  | EX |  |  |  | 43.24 | 43.19 |  | 43.14 | 43.32 |  |  | 43.26 |  |  | 43.41 |  | 43.40 | 43.29 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.06 |  |  | 56.96 |  |  |  | 57.18 |  |  |  |  | 0.21 |  |  |  |  | Grading |  |  | EX |  |  |  | 56.96 | 57.18 |  | 57.10 | 57.00 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.73, 0.7361 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.41 |  |  | 0.36 |  |  |  | 0.45 |  |  |  |  | 0.09 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.841 (5.835-5.846) x 3.547 /0.002 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 3.19 |  |  | 3.08 |  |  |  | 3.27 |  |  |  |  | 0.19 |  |  |  |  | E |  |  | EX |  |  |  | 3.08 | 3.13 |  | 3.22 | 3.12 |  |  | 3.27 |  |  | 3.27 |  | 3.26 | 3.19 |
| Spread |  |  | 0.01 ct, 1.10% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 3.23 |  |  | 2.96 |  |  |  | 3.52 |  |  |  |  | 0.55 |  |  |  |  |  |  |  | EX |  |  |  | 3.21 | 3.20 |  | 3.02 | 3.35 |  |  | 3.39 |  |  | 3.52 |  | 3.24 | 2.96 |
| AGS Spread |  |  | N/A ct, N/A% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.57 |  |  | 1.34 |  |  |  | 1.74 |  |  |  |  | 0.41 |  |  |  |  | E |  |  | EX |  |  |  | 1.42 | 1.45 |  | 1.54 | 1.61 |  |  | 1.49 |  |  | 1.42 |  | 1.54 | 1.72 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.74 | 1.71 |  | 1.70 | 1.73 |  |  | 1.63 |  |  | 1.54 |  | 1.51 | 1.34 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 55.01: |  |  | 54.07: |  |  |  | 56.09: |  |  |  |  | 2.02 |  |  |  |  | E |  |  | VG |  |  |  | 54.07: | 56.09: |  | 54.97: | 54.92: |  |  | 55.20: |  |  | 55.27: |  | 54.32: | 55.24: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 44.99 |  |  | 45.93 |  |  |  | 43.91 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 45.93 | 43.91 |  | 45.03 | 45.08 |  |  | 44.80 |  |  | 44.73 |  | 45.68 | 44.76 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 21.88 |  |  | 21.58 |  |  |  | 22.27 |  |  |  |  | 0.69 |  |  |  |  |  |  |  | EX |  |  |  | 21.89 | 22.27 |  | 21.83 | 21.65 |  |  | 21.58 |  |  | 21.97 |  | 21.72 | 22.15 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 40.96 |  |  | 40.17 |  |  |  | 41.54 |  |  |  |  | 1.37 |  |  |  |  |  |  |  | VG |  |  |  | 40.63 | 40.96 |  | 41.23 | 41.43 |  |  | 41.08 |  |  | 41.25 |  | 41.05 | 40.90 |
| 5.841 | 3.547 | 0.833 | 2.528 | 3.333 |  | 0.024 | 0.187 | 0.189 | 0.092 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 40.98 | 41.34 |  | 40.17 | 40.48 |  |  | 40.67 |  |  | 40.71 |  | 40.90 | 41.54 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 79.84 |  |  | 78.73 |  |  |  | 80.60 |  |  |  |  | 1.87 |  |  |  |  | E |  |  | EX |  |  |  | 79.84 | 80.60 |  | 80.56 | 79.77 |  |  | 80.15 |  |  | 79.84 |  | 79.63 | 79.73 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 79.34 | 78.73 |  | 79.50 | 79.61 |  |  | 80.04 |  |  | 80.18 |  | 79.61 | 80.26 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.06 |  |  | 41.80 |  |  |  | 42.31 |  |  |  |  | 0.51 |  |  |  |  |  |  |  | EX |  |  |  | 41.95 | 41.87 |  | 41.80 | 41.83 |  |  | 41.95 |  |  | 42.06 |  | 42.03 | 42.03 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.11 | 42.20 |  | 42.30 | 42.31 |  |  | 42.21 |  |  | 42.16 |  | 42.05 | 42.04 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.58 |  |  | 0.06 |  |  |  | 1.36 |  |  |  |  | 1.29 |  |  |  |  |  |  |  | VG |  |  |  | 0.83 | 0.13 |  | 0.23 | 0.23 |  |  | 0.06 |  |  | 0.89 |  | 0.89 | 1.36 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.833 |  |  | 0.821 |  |  |  | 0.842 |  |  |  |  | 0.021 |  |  |  |  | E |  |  | EX |  |  |  | 0.841 | 0.842 |  | 0.839 | 0.835 |  |  | 0.829 |  |  | 0.821 |  | 0.822 | 0.832 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.528 |  |  | 2.520 |  |  |  | 2.535 |  |  |  |  | 0.016 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.526 | 2.522 |  | 2.520 | 2.530 |  |  | 2.527 |  |  | 2.535 |  | 2.535 | 2.529 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.333 |  |  | 3.327 |  |  |  | 3.339 |  |  |  |  | 0.012 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.327 | 3.339 |  | 3.335 | 3.329 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.024 |  |  | 0.021 |  |  |  | 0.026 |  |  |  |  | 0.005 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.187 |  |  | 0.180 |  |  |  | 0.191 |  |  |  |  | 0.011 |  |  |  |  | E |  |  | EX |  |  |  | 0.180 | 0.183 |  | 0.188 | 0.182 |  |  | 0.191 |  |  | 0.191 |  | 0.190 | 0.186 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.189 |  |  | 0.173 |  |  |  | 0.205 |  |  |  |  | 0.032 |  |  |  |  |  |  |  | EX |  |  |  | 0.187 | 0.187 |  | 0.176 | 0.195 |  |  | 0.198 |  |  | 0.205 |  | 0.189 | 0.173 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.092 |  |  | 0.078 |  |  |  | 0.102 |  |  |  |  | 0.024 |  |  |  |  | E |  |  | EX |  |  |  | 0.083 | 0.085 |  | 0.090 | 0.094 |  |  | 0.087 |  |  | 0.083 |  | 0.090 | 0.101 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.102 | 0.100 |  | 0.099 | 0.101 |  |  | 0.095 |  |  | 0.090 |  | 0.088 | 0.078 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 33.53 |  |  | 33.51 |  |  |  | 33.57 |  |  |  |  | 0.06 |  |  |  |  |  |  |  |  |  |  |  | 33.57 | 33.52 |  | 33.52 | 33.51 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.98 |  |  | 40.95 |  |  |  | 41.00 |  |  |  |  | 0.05 |  |  |  |  |  |  |  |  |  |  |  | 40.96 | 40.95 |  | 40.99 | 41.00 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 8.92 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 12.89 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.002 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | 0.40 |  |  |  |  | 0.08 | 0.77 |  |  |  | 0.72 |  |  | 0.14 | 0.14 |  | -0.08 |  |  | Crown, ° |  | 0.01 |  |  |  |  |  |  | EX |  | 1.10 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.83 |  |  | 0.53 |  |  |  |  | 0.31 | 0.54 |  |  |  | 0.79 |  |  | 1.03 | 1.03 |  | 1.28 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.3 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.55 |  |  | 0.17 |  |  |  |  | -0.12 | 0.37 |  |  |  | -0.18 |  |  | 0.21 | -0.07 |  | -0.07 |  |  | Pavilion, ° |  | -0.05 |  |  |  |  |  |  | EX |  | -0.53 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.16 |  |  | 0.85 |  |  |  |  | -1.06 | -0.26 |  |  |  | -0.24 |  |  | 0.34 | -0.22 |  | 1.10 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.1 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | -0.15 |  |  | 0.41 |  |  |  |  | -0.12 | -0.07 |  |  |  | 0.46 |  |  | 0.31 | -0.25 |  | 0.05 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.25 |  |  | -0.53 |  |  |  |  | 0.28 | -0.31 |  |  |  | -0.16 |  |  | -0.26 | -0.19 |  | -0.03 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.24 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.014 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.20 ± 0.19, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.012 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.12 ± 0.23, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.007 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.20 %, 0.012 mm |  |  |  |  |  |