| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  | 02.08.2008 |  |  |  | Diameter, mm |  |  | 5.812 |  |  | 5.804 |  |  |  | 5.821 |  |  |  |  | 0.29% |  |  |  |  | E |  |  | EX |  |  |  | 5.813 | 5.815 |  | 5.810 | 5.811 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 39.05 |  |  | 38.91 |  |  |  | 39.17 |  |  |  |  | 0.26 |  |  |  |  | Grading |  |  | EX |  |  |  | 39.08 | 38.91 |  | 38.99 | 39.09 |  |  | 39.12 |  | 39.17 |  | 39.10 | 38.92 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 39.98 |  |  | 39.84 |  |  |  | 40.17 |  |  |  |  | 0.32 |  |  |  |  | Grading |  |  | EX |  |  |  | 39.99 | 40.12 |  | 40.17 | 39.97 |  |  | 39.91 |  | 39.84 |  | 39.87 | 39.95 |
| Model |  |  |  | Simple |  |  |  |  |  |  |  |  | Total height, % |  |  | 60.53 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  |  | Makoed A.G. |  |  |  |  |  |  |  |  | Crown height, % |  |  | 15.88 |  |  | 15.79 |  |  |  | 16.06 |  |  |  |  | 0.28 |  |  |  |  | E |  |  | EX |  |  |  | 16.06 | 15.80 |  | 15.79 | 15.79 |  |  | 15.89 |  | 15.93 |  | 15.91 | 15.89 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 41.74 |  |  | 41.64 |  |  |  | 41.83 |  |  |  |  | 0.20 |  |  |  |  | N/A |  |  | EX |  |  |  | 41.64 | 41.73 |  | 41.76 | 41.72 |  |  | 41.83 |  | 41.76 |  | 41.82 | 41.66 |
| Calculated weight, ct |  |  |  | 0.74, 0.7431 |  |  |  |  |  |  |  |  | Table, % |  |  | 60.95 |  |  | 60.78 |  |  |  | 61.05 |  |  |  |  | 0.27 |  |  |  |  | Grading |  |  | EX |  |  |  | 60.78 | 60.99 |  | 61.05 | 60.98 |  |  |  |  |  |  |  |  |
| Measurements |  |  |  | 5.812 (5.804 -5.821) x 3.518 /0.010 mm |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.39 |  |  | 0.33 |  |  |  | 0.41 |  |  |  |  | 0.08 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Spread |  |  |  | -0.01 ct, -1.78 % |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 2.90 |  |  | 2.78 |  |  |  | 3.02 |  |  |  |  | 0.25 |  |  |  |  | E |  |  | EX |  |  |  | 2.83 | 2.99 |  | 2.98 | 3.02 |  |  | 2.80 |  | 2.84 |  | 2.78 | 2.97 |
| AGS Spread |  |  |  | N/A ct, N/A % |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 2.85 |  |  | 2.65 |  |  |  | 3.09 |  |  |  |  | 0.44 |  |  |  |  |  |  |  | EX |  |  |  | 2.80 | 3.05 |  | 2.79 | 2.65 |  |  | 3.07 |  | 2.66 |  | 2.71 | 3.09 |
| Extra Facet / Nat |  |  |  | No |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 0.95 |  |  | 0.72 |  |  |  | 1.17 |  |  |  |  | 0.45 |  |  |  |  | E |  |  | EX |  |  |  | 0.72 | 0.96 |  | 0.95 | 1.17 |  |  | 1.09 |  | 1.16 |  | 0.87 | 0.85 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.92 | 1.03 |  | 0.86 | 0.88 |  |  | 0.93 |  | 0.79 |  | 1.02 | 1.00 |
| Width |  | Length | Ratio (L/W) |  | Diameter Minimum |  | Diameter Maximum | Diameter Average |  | Total height |  |  | Star: |  |  | 61.69: |  |  | 60.59: |  |  |  | 63.53: |  |  |  |  | 2.94 |  |  |  |  | E |  |  | VG |  |  |  | 61.80: | 62.10: |  | 61.24: | 61.25: |  |  | 63.53: |  | 60.98: |  | 60.59: | 62.01: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 38.31 |  |  | 39.41 |  |  |  | 36.47 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 38.20 | 37.90 |  | 38.76 | 38.75 |  |  | 36.47 |  | 39.02 |  | 39.41 | 37.99 |
| 5.804 mm |  | 5.821 mm | 1.003 |  | 5.804 mm |  | 5.821 mm | 5.812 mm |  | 3.518 mm |  |  | Star angle, ° |  |  | 25.81 |  |  | 25.56 |  |  |  | 26.10 |  |  |  |  | 0.53 |  |  |  |  |  |  |  | EX |  |  |  | 25.87 | 25.98 |  | 25.63 | 25.76 |  |  | 26.10 |  | 25.78 |  | 25.78 | 25.56 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper girdle angle, ° |  |  | 49.00 |  |  | 48.50 |  |  |  | 49.42 |  |  |  |  | 0.92 |  |  |  |  |  |  |  | EX |  |  |  | 48.80 | 49.28 |  | 48.64 | 48.50 |  |  | 49.01 |  | 49.21 |  | 48.74 | 49.06 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 49.09 | 49.25 |  | 48.89 | 49.06 |  |  | 48.95 |  | 48.98 |  | 49.42 | 49.06 |
| Crown height |  | Pavilion depth | Table |  | Culet |  | Girdle |  |  |  |  |  | Length girdle facet, % |  |  | 80.46 |  |  | 78.99 |  |  |  | 81.69 |  |  |  |  | 2.70 |  |  |  |  | E |  |  | EX |  |  |  | 79.58 | 80.42 |  | 80.34 | 80.78 |  |  | 80.85 |  | 81.34 |  | 80.94 | 81.69 |
|  |  |  |  |  |  |  | Bezel | Bone |  | Valley |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 81.51 | 81.17 |  | 81.49 | 80.19 |  |  | 79.68 |  | 79.09 |  | 79.23 | 78.99 |
| 0.923 mm |  | 2.426 mm | 3.542 mm |  | 0.022 mm |  | 0.169 mm | 0.166 mm |  | 0.055 mm |  |  | Lower girdle angle / Halves angle, ° |  |  | 41.05 |  |  | 40.87 |  |  |  | 41.34 |  |  |  |  | 0.47 |  |  |  |  |  |  |  | EX |  |  |  | 41.16 | 41.13 |  | 41.34 | 41.26 |  |  | 41.14 |  | 41.01 |  | 41.01 | 40.94 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 40.97 | 40.87 |  | 40.90 | 40.88 |  |  | 41.01 |  | 41.06 |  | 41.07 | 41.06 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.81 |  |  | 0.20 |  |  |  | 1.46 |  |  |  |  | 1.26 |  |  |  |  |  |  |  | VG |  |  |  | 0.46 | 0.78 |  | 0.48 | 0.56 |  |  | 1.28 |  | 1.22 |  | 1.46 | 0.20 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.923 |  |  | 0.917 |  |  |  | 0.934 |  |  |  |  | 0.016 |  |  |  |  | E |  |  | EX |  |  |  | 0.934 | 0.918 |  | 0.917 | 0.918 |  |  | 0.924 |  | 0.926 |  | 0.924 | 0.923 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.426 |  |  | 2.420 |  |  |  | 2.431 |  |  |  |  | 0.012 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.420 | 2.425 |  | 2.427 | 2.424 |  |  | 2.431 |  | 2.427 |  | 2.430 | 2.421 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.542 |  |  | 3.532 |  |  |  | 3.548 |  |  |  |  | 0.016 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.532 | 3.544 |  | 3.548 | 3.544 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.022 |  |  | 0.019 |  |  |  | 0.024 |  |  |  |  | 0.005 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.169 |  |  | 0.161 |  |  |  | 0.176 |  |  |  |  | 0.014 |  |  |  |  | E |  |  | EX |  |  |  | 0.164 | 0.174 |  | 0.173 | 0.176 |  |  | 0.163 |  | 0.165 |  | 0.161 | 0.173 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.166 |  |  | 0.154 |  |  |  | 0.180 |  |  |  |  | 0.026 |  |  |  |  |  |  |  | EX |  |  |  | 0.163 | 0.177 |  | 0.162 | 0.154 |  |  | 0.179 |  | 0.155 |  | 0.158 | 0.180 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.055 |  |  | 0.042 |  |  |  | 0.068 |  |  |  |  | 0.026 |  |  |  |  | E |  |  | EX |  |  |  | 0.042 | 0.056 |  | 0.055 | 0.068 |  |  | 0.063 |  | 0.068 |  | 0.050 | 0.050 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.053 | 0.060 |  | 0.050 | 0.051 |  |  | 0.054 |  | 0.046 |  | 0.059 | 0.058 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 39.05 |  |  | 39.01 |  |  |  | 39.10 |  |  |  |  | 0.10 |  |  |  |  |  |  |  |  |  |  |  | 39.10 | 39.04 |  | 39.05 | 39.01 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 39.98 |  |  | 39.95 |  |  |  | 40.02 |  |  |  |  | 0.07 |  |  |  |  |  |  |  |  |  |  |  | 39.95 | 39.98 |  | 40.02 | 39.96 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 2.47 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | MIC, mm |  |  |  |  | 5.794 |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 7.91 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.010 |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  | 1 |  |  |  | 2 |  |  |  |  | 3 | 4 |  |  | 5 |  |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  | 0.00 |  |  |  | -0.56 |  |  |  |  | -0.10 | -0.15 |  |  | -0.65 |  |  |  | -0.74 | -0.83 |  | -0.05 |  |  | Crown, ° |  | 0.12 |  |  |  |  |  | EX |  | -0.97 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  | 0.46 |  |  |  | 0.22 |  |  |  |  | 0.38 | 0.41 |  |  | 0.63 |  |  |  | 0.48 | 0.64 |  | 0.16 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  | 0.3 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  | -0.61 |  |  |  | 0.89 |  |  |  |  | -0.49 | -0.71 |  |  | 0.34 |  |  |  | 0.72 | -0.50 |  | 0.81 |  |  | Pavilion, ° |  | 0.10 |  |  |  |  |  | EX |  | 1.17 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.97 |  |  |  | 0.21 |  |  |  |  | -0.20 | 0.85 |  |  | -0.12 |  |  |  | 0.64 | 0.50 |  | 0.58 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  | 0.3 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  | -0.27 |  |  |  | -0.47 |  |  |  |  | 1.17 | -0.30 |  |  | 0.18 |  |  |  | -0.05 | 0.31 |  | -0.17 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.23 |  |  |  | -0.55 |  |  |  |  | 0.82 | -0.73 |  |  | 0.72 |  |  |  | 0.39 | -0.04 |  | 0.31 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  |  | G |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet offset by table axis |  |  |  |  | 0.28 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.016 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table offset by table axis |  |  |  |  | 0.10 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.006 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet offset by table axis |  |  |  |  | 0.33 ± 0.23, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.019 ± 0.014, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  | 0.08 %, 0.005 mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |