| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  | 02.08.2008 |  |  |  | Diameter, mm |  |  | 5.803 |  |  | 5.795 |  |  |  | 5.808 |  |  |  |  | 0.23% |  |  |  |  | E |  |  | EX |  |  |  | 5.805 | 5.804 |  | 5.803 | 5.801 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 37.52 |  |  | 37.39 |  |  |  | 37.61 |  |  |  |  | 0.23 |  |  |  |  | Grading |  |  | EX |  |  |  | 37.39 | 37.47 |  | 37.54 | 37.61 |  |  | 37.61 |  | 37.55 |  | 37.49 | 37.47 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.39 |  |  | 40.32 |  |  |  | 40.45 |  |  |  |  | 0.14 |  |  |  |  | Grading |  |  | EX |  |  |  | 40.44 | 40.39 |  | 40.37 | 40.35 |  |  | 40.45 |  | 40.45 |  | 40.32 | 40.32 |
| Model |  |  |  | Simple |  |  |  |  |  |  |  |  | Total height, % |  |  | 61.82 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  |  | Makoed A.G. |  |  |  |  |  |  |  |  | Crown height, % |  |  | 16.42 |  |  | 16.30 |  |  |  | 16.54 |  |  |  |  | 0.24 |  |  |  |  | E |  |  | EX |  |  |  | 16.30 | 16.40 |  | 16.46 | 16.51 |  |  | 16.54 |  | 16.42 |  | 16.36 | 16.36 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 42.38 |  |  | 42.20 |  |  |  | 42.61 |  |  |  |  | 0.41 |  |  |  |  | N/A |  |  | EX |  |  |  | 42.61 | 42.46 |  | 42.32 | 42.20 |  |  | 42.38 |  | 42.42 |  | 42.29 | 42.37 |
| Calculated weight, ct |  |  |  | 0.74, 0.7465 |  |  |  |  |  |  |  |  | Table, % |  |  | 57.26 |  |  | 57.22 |  |  |  | 57.29 |  |  |  |  | 0.07 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.29 | 57.26 |  | 57.28 | 57.22 |  |  |  |  |  |  |  |  |
| Measurements |  |  |  | 5.803 (5.795 -5.808) x 3.587 /0.004 mm |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.43 |  |  | 0.38 |  |  |  | 0.47 |  |  |  |  | 0.09 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Spread |  |  |  | -0.02 ct, -2.25 % |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 3.01 |  |  | 2.90 |  |  |  | 3.17 |  |  |  |  | 0.27 |  |  |  |  | E |  |  | EX |  |  |  | 2.90 | 2.98 |  | 3.04 | 3.08 |  |  | 2.90 |  | 2.94 |  | 3.17 | 3.08 |
| AGS Spread |  |  |  | N/A ct, N/A % |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 3.00 |  |  | 2.85 |  |  |  | 3.22 |  |  |  |  | 0.36 |  |  |  |  |  |  |  | EX |  |  |  | 2.94 | 2.95 |  | 3.05 | 2.96 |  |  | 3.22 |  | 3.04 |  | 2.85 | 2.98 |
| Extra Facet / Nat |  |  |  | No |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.25 |  |  | 1.06 |  |  |  | 1.41 |  |  |  |  | 0.34 |  |  |  |  | E |  |  | EX |  |  |  | 1.22 | 1.11 |  | 1.34 | 1.23 |  |  | 1.28 |  | 1.37 |  | 1.34 | 1.06 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.24 | 1.23 |  | 1.22 | 1.41 |  |  | 1.31 |  | 1.12 |  | 1.30 | 1.22 |
| Width |  | Length | Ratio (L/W) |  | Diameter Minimum |  | Diameter Maximum | Diameter Average |  | Total height |  |  | Star: |  |  | 54.57: |  |  | 53.26: |  |  |  | 55.49: |  |  |  |  | 2.23 |  |  |  |  | E |  |  | VG |  |  |  | 54.88: | 53.26: |  | 54.35: | 55.49: |  |  | 55.10: |  | 54.56: |  | 54.38: | 54.51: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 45.43 |  |  | 46.74 |  |  |  | 44.51 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 45.12 | 46.74 |  | 45.65 | 44.51 |  |  | 44.90 |  | 45.44 |  | 45.62 | 45.49 |
| 5.795 mm |  | 5.808 mm | 1.002 |  | 5.795 mm |  | 5.808 mm | 5.803 mm |  | 3.587 mm |  |  | Star angle, ° |  |  | 24.97 |  |  | 24.80 |  |  |  | 25.21 |  |  |  |  | 0.41 |  |  |  |  |  |  |  | EX |  |  |  | 25.04 | 24.80 |  | 24.95 | 25.21 |  |  | 24.88 |  | 24.89 |  | 25.01 | 24.97 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper girdle angle, ° |  |  | 45.12 |  |  | 44.66 |  |  |  | 45.70 |  |  |  |  | 1.04 |  |  |  |  |  |  |  | VG |  |  |  | 45.21 | 45.11 |  | 44.75 | 45.06 |  |  | 45.20 |  | 45.09 |  | 45.18 | 45.70 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 44.89 | 45.18 |  | 44.75 | 45.16 |  |  | 45.14 |  | 45.56 |  | 44.66 | 45.26 |
| Crown height |  | Pavilion depth | Table |  | Culet |  | Girdle |  |  |  |  |  | Length girdle facet, % |  |  | 80.80 |  |  | 80.19 |  |  |  | 81.40 |  |  |  |  | 1.20 |  |  |  |  | E |  |  | EX |  |  |  | 81.15 | 80.55 |  | 81.01 | 80.56 |  |  | 80.92 |  | 80.77 |  | 80.47 | 81.02 |
|  |  |  |  |  |  |  | Bezel | Bone |  | Valley |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 81.40 | 80.89 |  | 81.17 | 80.73 |  |  | 80.43 |  | 80.62 |  | 80.86 | 80.19 |
| 0.953 mm |  | 2.459 mm | 3.323 mm |  | 0.025 mm |  | 0.175 mm | 0.174 mm |  | 0.073 mm |  |  | Lower girdle angle / Halves angle, ° |  |  | 41.45 |  |  | 41.37 |  |  |  | 41.55 |  |  |  |  | 0.18 |  |  |  |  |  |  |  | EX |  |  |  | 41.46 | 41.48 |  | 41.44 | 41.46 |  |  | 41.41 |  | 41.38 |  | 41.43 | 41.49 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.51 | 41.55 |  | 41.48 | 41.40 |  |  | 41.37 |  | 41.40 |  | 41.42 | 41.52 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.54 |  |  | 0.26 |  |  |  | 0.77 |  |  |  |  | 0.51 |  |  |  |  |  |  |  | EX |  |  |  | 0.28 | 0.77 |  | 0.75 | 0.26 |  |  | 0.37 |  | 0.73 |  | 0.54 | 0.64 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.953 |  |  | 0.946 |  |  |  | 0.960 |  |  |  |  | 0.014 |  |  |  |  | E |  |  | EX |  |  |  | 0.946 | 0.952 |  | 0.955 | 0.958 |  |  | 0.960 |  | 0.953 |  | 0.949 | 0.950 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.459 |  |  | 2.449 |  |  |  | 2.473 |  |  |  |  | 0.024 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.473 | 2.464 |  | 2.456 | 2.449 |  |  | 2.459 |  | 2.462 |  | 2.454 | 2.459 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.323 |  |  | 3.320 |  |  |  | 3.324 |  |  |  |  | 0.004 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.324 | 3.323 |  | 3.324 | 3.320 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.025 |  |  | 0.022 |  |  |  | 0.027 |  |  |  |  | 0.005 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.175 |  |  | 0.168 |  |  |  | 0.184 |  |  |  |  | 0.016 |  |  |  |  | E |  |  | EX |  |  |  | 0.169 | 0.173 |  | 0.176 | 0.179 |  |  | 0.168 |  | 0.170 |  | 0.184 | 0.179 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.174 |  |  | 0.166 |  |  |  | 0.187 |  |  |  |  | 0.021 |  |  |  |  |  |  |  | EX |  |  |  | 0.171 | 0.171 |  | 0.177 | 0.172 |  |  | 0.187 |  | 0.176 |  | 0.166 | 0.173 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.073 |  |  | 0.062 |  |  |  | 0.082 |  |  |  |  | 0.020 |  |  |  |  | E |  |  | EX |  |  |  | 0.071 | 0.064 |  | 0.078 | 0.071 |  |  | 0.074 |  | 0.079 |  | 0.078 | 0.062 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.072 | 0.072 |  | 0.071 | 0.082 |  |  | 0.076 |  | 0.065 |  | 0.075 | 0.071 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 37.52 |  |  | 37.50 |  |  |  | 37.54 |  |  |  |  | 0.04 |  |  |  |  |  |  |  |  |  |  |  | 37.50 | 37.51 |  | 37.51 | 37.54 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.39 |  |  | 40.34 |  |  |  | 40.45 |  |  |  |  | 0.11 |  |  |  |  |  |  |  |  |  |  |  | 40.45 | 40.42 |  | 40.34 | 40.34 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 6.27 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | MIC, mm |  |  |  |  | 5.791 |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 5.43 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.004 |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  | 1 |  |  |  | 2 |  |  |  |  | 3 | 4 |  |  | 5 |  |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  | -0.00 |  |  |  | 0.04 |  |  |  |  | 0.20 | 0.60 |  |  | 0.25 |  |  |  | 0.19 | 0.37 |  | 0.03 |  |  | Crown, ° |  | 0.04 |  |  |  |  |  | EX |  | 0.93 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  | 0.28 |  |  |  | 0.81 |  |  |  |  | 0.94 | 0.86 |  |  | 0.62 |  |  |  | 0.92 | 0.92 |  | 0.67 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  | 0.2 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  | 0.16 |  |  |  | 0.17 |  |  |  |  | 0.01 | 0.41 |  |  | 0.01 |  |  |  | 0.25 | -0.39 |  | 0.43 |  |  | Pavilion, ° |  | 0.01 |  |  |  |  |  | EX |  | 0.37 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.42 |  |  |  | 0.05 |  |  |  |  | -0.59 | 0.43 |  |  | -0.39 |  |  |  | 0.93 | -0.80 |  | 0.47 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  | 0.1 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  | 0.05 |  |  |  | -0.07 |  |  |  |  | 0.20 | -0.09 |  |  | 0.03 |  |  |  | 0.13 | -0.27 |  | -0.31 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.30 |  |  |  | -0.20 |  |  |  |  | 0.24 | 0.37 |  |  | -0.20 |  |  |  | -0.04 | 0.31 |  | -0.29 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  |  | V |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet offset by table axis |  |  |  |  | 0.18 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.010 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table offset by table axis |  |  |  |  | 0.11 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.007 ± 0.012, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet offset by table axis |  |  |  |  | 0.26 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.015 ± 0.014, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  | 0.06 %, 0.004 mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |