| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.766 |  |  | 5.727 |  |  |  | 5.778 |  |  |  |  | 0.90% |  |  |  |  | E |  |  | VG |  |  |  | 5.777 | 5.776 |  | 5.761 | 5.769 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.58 |  |  | 34.50 |  |  |  | 34.74 |  |  |  |  | 0.24 |  |  |  |  | Grading |  |  | EX |  |  |  | 34.56 | 34.57 |  | 34.65 | 34.50 |  |  | 34.51 |  |  | 34.54 |  | 34.74 | 34.53 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.74 |  |  | 41.64 |  |  |  | 41.83 |  |  |  |  | 0.19 |  |  |  |  | Grading |  |  | EX |  |  |  | 41.73 | 41.73 |  | 41.64 | 41.79 |  |  | 41.83 |  |  | 41.71 |  | 41.76 | 41.76 |
| Model |  |  | st2 |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 62.90 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 15.47 |  |  | 15.35 |  |  |  | 15.63 |  |  |  |  | 0.29 |  |  |  |  | E |  |  | EX |  |  |  | 15.35 | 15.44 |  | 15.35 | 15.41 |  |  | 15.55 |  |  | 15.63 |  | 15.51 | 15.51 |
| Report date |  |  | 10.12.2007 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 44.50 |  |  | 44.30 |  |  |  | 44.70 |  |  |  |  | 0.40 |  |  |  |  | N/A |  |  | EX |  |  |  | 44.70 | 44.69 |  | 44.30 | 44.48 |  |  | 44.46 |  |  | 44.38 |  | 44.48 | 44.50 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 55.23 |  |  | 55.07 |  |  |  | 55.41 |  |  |  |  | 0.34 |  |  |  |  | Grading |  |  | EX |  |  |  | 55.28 | 55.07 |  | 55.41 | 55.14 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.73, 0.7288 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.39 |  |  | 0.29 |  |  |  | 0.44 |  |  |  |  | 0.15 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.766 (5.727-5.778) x 3.626 /0.002 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 2.91 |  |  | 2.71 |  |  |  | 3.25 |  |  |  |  | 0.55 |  |  |  |  | E |  |  | EX |  |  |  | 2.80 | 2.71 |  | 3.25 | 3.00 |  |  | 2.86 |  |  | 2.84 |  | 2.90 | 2.89 |
| Spread |  |  | -0.02 ct, -2.86% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 3.25 |  |  | 3.00 |  |  |  | 3.69 |  |  |  |  | 0.70 |  |  |  |  |  |  |  | EX |  |  |  | 3.21 | 3.11 |  | 3.69 | 3.24 |  |  | 3.35 |  |  | 3.22 |  | 3.00 | 3.20 |
| AGS Spread |  |  | -0.02 ct, -3.16% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.45 |  |  | 1.21 |  |  |  | 2.41 |  |  |  |  | 1.20 |  |  |  |  | E |  |  | VG |  |  |  | 1.34 | 1.34 |  | 1.21 | 1.45 |  |  | 2.41 |  |  | 2.05 |  | 1.28 | 1.33 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.40 | 1.27 |  | 1.39 | 1.39 |  |  | 1.37 |  |  | 1.41 |  | 1.21 | 1.38 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 55.19: |  |  | 54.13: |  |  |  | 56.46: |  |  |  |  | 2.33 |  |  |  |  | E |  |  | VG |  |  |  | 55.16: | 54.73: |  | 55.13: | 55.91: |  |  | 56.46: |  |  | 54.46: |  | 54.13: | 55.56: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 44.81 |  |  | 45.87 |  |  |  | 43.54 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 44.84 | 45.27 |  | 44.87 | 44.09 |  |  | 43.54 |  |  | 45.54 |  | 45.87 | 44.44 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 23.64 |  |  | 23.53 |  |  |  | 23.81 |  |  |  |  | 0.28 |  |  |  |  |  |  |  | EX |  |  |  | 23.81 | 23.59 |  | 23.69 | 23.68 |  |  | 23.63 |  |  | 23.60 |  | 23.60 | 23.53 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 41.71 |  |  | 41.52 |  |  |  | 42.13 |  |  |  |  | 0.61 |  |  |  |  |  |  |  | EX |  |  |  | 41.72 | 41.72 |  | 41.81 | 41.52 |  |  | 41.53 |  |  | 42.13 |  | 41.63 | 41.70 |
| 5.766 | 3.626 | 0.892 | 2.566 | 3.184 |  | 0.023 | 0.168 | 0.188 | 0.084 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.63 | 41.68 |  | 41.69 | 41.73 |  |  | 41.66 |  |  | 41.75 |  | 41.81 | 41.69 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 80.05 |  |  | 78.74 |  |  |  | 80.98 |  |  |  |  | 2.24 |  |  |  |  | E |  |  | EX |  |  |  | 80.17 | 79.92 |  | 80.06 | 79.84 |  |  | 78.74 |  |  | 79.75 |  | 80.50 | 80.75 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 80.48 | 80.98 |  | 80.07 | 80.45 |  |  | 80.44 |  |  | 79.70 |  | 79.60 | 79.41 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.74 |  |  | 42.60 |  |  |  | 42.98 |  |  |  |  | 0.39 |  |  |  |  |  |  |  | EX |  |  |  | 42.60 | 42.63 |  | 42.75 | 42.62 |  |  | 42.83 |  |  | 42.98 |  | 42.81 | 42.85 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.75 | 42.74 |  | 42.66 | 42.67 |  |  | 42.78 |  |  | 42.76 |  | 42.79 | 42.67 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.28 |  |  | 0.02 |  |  |  | 0.52 |  |  |  |  | 0.50 |  |  |  |  |  |  |  | EX |  |  |  | 0.24 | 0.08 |  | 0.44 | 0.02 |  |  | 0.35 |  |  | 0.10 |  | 0.51 | 0.52 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.892 |  |  | 0.885 |  |  |  | 0.901 |  |  |  |  | 0.017 |  |  |  |  | E |  |  | EX |  |  |  | 0.885 | 0.890 |  | 0.885 | 0.889 |  |  | 0.897 |  |  | 0.901 |  | 0.894 | 0.894 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.566 |  |  | 2.554 |  |  |  | 2.577 |  |  |  |  | 0.023 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.577 | 2.577 |  | 2.554 | 2.564 |  |  | 2.563 |  |  | 2.559 |  | 2.565 | 2.566 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.184 |  |  | 3.175 |  |  |  | 3.195 |  |  |  |  | 0.019 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.187 | 3.175 |  | 3.195 | 3.179 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.023 |  |  | 0.017 |  |  |  | 0.025 |  |  |  |  | 0.009 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.168 |  |  | 0.156 |  |  |  | 0.188 |  |  |  |  | 0.031 |  |  |  |  | E |  |  | EX |  |  |  | 0.161 | 0.156 |  | 0.188 | 0.173 |  |  | 0.165 |  |  | 0.164 |  | 0.167 | 0.166 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.188 |  |  | 0.173 |  |  |  | 0.213 |  |  |  |  | 0.040 |  |  |  |  |  |  |  | EX |  |  |  | 0.185 | 0.179 |  | 0.213 | 0.187 |  |  | 0.193 |  |  | 0.186 |  | 0.173 | 0.185 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.084 |  |  | 0.069 |  |  |  | 0.139 |  |  |  |  | 0.069 |  |  |  |  | E |  |  | VG |  |  |  | 0.077 | 0.077 |  | 0.070 | 0.083 |  |  | 0.139 |  |  | 0.118 |  | 0.074 | 0.077 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.081 | 0.073 |  | 0.080 | 0.080 |  |  | 0.079 |  |  | 0.082 |  | 0.069 | 0.080 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.58 |  |  | 34.51 |  |  |  | 34.70 |  |  |  |  | 0.18 |  |  |  |  |  |  |  |  |  |  |  | 34.53 | 34.56 |  | 34.70 | 34.51 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.74 |  |  | 41.70 |  |  |  | 41.78 |  |  |  |  | 0.08 |  |  |  |  |  |  |  |  |  |  |  | 41.78 | 41.72 |  | 41.70 | 41.77 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 13.06 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 7.38 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.002 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | -0.12 |  |  |  |  | 0.33 | -0.26 |  |  |  | 0.38 |  |  | 0.43 | -0.01 |  | -0.13 |  |  | Crown, ° |  | -0.11 |  |  |  |  |  |  | EX |  | 1.33 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.24 |  |  | -0.04 |  |  |  |  | -0.11 | -0.28 |  |  |  | 0.03 |  |  | 0.33 | 0.50 |  | 0.39 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.4 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.47 |  |  | -0.05 |  |  |  |  | -0.10 | -0.18 |  |  |  | -0.62 |  |  | 1.33 | -1.00 |  | -0.05 |  |  | Pavilion, ° |  | -0.60 |  |  |  | Painting |  |  | EX |  | -1.95 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.64 |  |  | -0.62 |  |  |  |  | 0.42 | -0.33 |  |  |  | 0.03 |  |  | 0.38 | -0.47 |  | 0.66 |  |  | Pavilion, notch. |  | 0.2, Very small |  |  |  |  |  |  |  |  | 0.5 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | -1.28 |  |  | -0.61 |  |  |  |  | -1.43 | 0.22 |  |  |  | -0.51 |  |  | 1.89 | -1.59 |  | 0.28 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -1.63 |  |  | -1.06 |  |  |  |  | -0.08 | -1.95 |  |  |  | 0.16 |  |  | -0.91 | -0.05 |  | -1.13 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.29 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.017 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.55 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.032 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.37 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.022 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.46 %, 0.027 mm |  |  |  |  |  |