| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.727 |  |  | 5.720 |  |  |  | 5.739 |  |  |  |  | 0.34% |  |  |  |  | E |  |  | EX |  |  |  | 5.722 | 5.731 |  | 5.730 | 5.728 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 36.15 |  |  | 35.96 |  |  |  | 36.48 |  |  |  |  | 0.53 |  |  |  |  | Grading |  |  | EX |  |  |  | 36.05 | 35.96 |  | 36.04 | 36.29 |  |  | 36.10 |  |  | 36.18 |  | 36.48 | 36.08 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.40 |  |  | 40.26 |  |  |  | 40.55 |  |  |  |  | 0.29 |  |  |  |  | Grading |  |  | EX |  |  |  | 40.51 | 40.37 |  | 40.33 | 40.26 |  |  | 40.34 |  |  | 40.36 |  | 40.55 | 40.50 |
| Model |  |  | st3 |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 61.26 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 15.62 |  |  | 15.41 |  |  |  | 15.80 |  |  |  |  | 0.39 |  |  |  |  | E |  |  | EX |  |  |  | 15.62 | 15.80 |  | 15.78 | 15.74 |  |  | 15.56 |  |  | 15.41 |  | 15.60 | 15.43 |
| Report date |  |  | 10.12.2007 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 42.38 |  |  | 42.13 |  |  |  | 42.63 |  |  |  |  | 0.50 |  |  |  |  | N/A |  |  | EX |  |  |  | 42.30 | 42.46 |  | 42.34 | 42.13 |  |  | 42.34 |  |  | 42.34 |  | 42.63 | 42.52 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.26 |  |  | 57.13 |  |  |  | 57.40 |  |  |  |  | 0.27 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.13 | 57.26 |  | 57.27 | 57.40 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.71, 0.7095 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.41 |  |  | 0.30 |  |  |  | 0.50 |  |  |  |  | 0.20 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.727 (5.720-5.739) x 3.509 /0.018 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 3.26 |  |  | 3.00 |  |  |  | 3.52 |  |  |  |  | 0.51 |  |  |  |  | E |  |  | EX |  |  |  | 3.34 | 3.00 |  | 3.13 | 3.40 |  |  | 3.37 |  |  | 3.52 |  | 3.04 | 3.32 |
| Spread |  |  | -0.01 ct, -2.03% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 3.14 |  |  | 2.80 |  |  |  | 3.35 |  |  |  |  | 0.55 |  |  |  |  |  |  |  | EX |  |  |  | 3.20 | 3.27 |  | 3.35 | 3.15 |  |  | 2.92 |  |  | 3.16 |  | 2.80 | 3.32 |
| AGS Spread |  |  | -0.02 ct, -2.35% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.49 |  |  | 1.28 |  |  |  | 1.85 |  |  |  |  | 0.57 |  |  |  |  | E |  |  | EX |  |  |  | 1.39 | 1.32 |  | 1.45 | 1.60 |  |  | 1.45 |  |  | 1.73 |  | 1.55 | 1.35 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.46 | 1.50 |  | 1.61 | 1.36 |  |  | 1.28 |  |  | 1.37 |  | 1.63 | 1.85 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 52.77: |  |  | 52.07: |  |  |  | 53.86: |  |  |  |  | 1.80 |  |  |  |  | E |  |  | EX |  |  |  | 53.19: | 52.69: |  | 53.86: | 52.82: |  |  | 52.07: |  |  | 52.10: |  | 52.49: | 52.95: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 47.23 |  |  | 47.93 |  |  |  | 46.14 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 46.81 | 47.31 |  | 46.14 | 47.18 |  |  | 47.93 |  |  | 47.90 |  | 47.51 | 47.05 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 23.57 |  |  | 23.19 |  |  |  | 24.02 |  |  |  |  | 0.83 |  |  |  |  |  |  |  | EX |  |  |  | 23.69 | 23.19 |  | 23.65 | 24.02 |  |  | 23.42 |  |  | 23.48 |  | 23.37 | 23.70 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 43.32 |  |  | 42.90 |  |  |  | 43.72 |  |  |  |  | 0.82 |  |  |  |  |  |  |  | EX |  |  |  | 43.04 | 42.94 |  | 43.32 | 43.41 |  |  | 43.43 |  |  | 43.59 |  | 42.90 | 42.92 |
| 5.727 | 3.509 | 0.895 | 2.427 | 3.280 |  | 0.023 | 0.187 | 0.180 | 0.086 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 43.51 | 43.72 |  | 43.55 | 43.41 |  |  | 43.08 |  |  | 43.55 |  | 43.41 | 43.43 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 81.13 |  |  | 80.18 |  |  |  | 82.07 |  |  |  |  | 1.90 |  |  |  |  | E |  |  | EX |  |  |  | 81.52 | 81.16 |  | 82.07 | 81.85 |  |  | 81.46 |  |  | 80.50 |  | 80.78 | 80.18 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 80.75 | 80.30 |  | 81.38 | 80.81 |  |  | 81.49 |  |  | 81.76 |  | 81.29 | 80.81 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 41.51 |  |  | 41.32 |  |  |  | 41.64 |  |  |  |  | 0.31 |  |  |  |  |  |  |  | EX |  |  |  | 41.59 | 41.55 |  | 41.41 | 41.39 |  |  | 41.46 |  |  | 41.41 |  | 41.37 | 41.32 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.52 | 41.62 |  | 41.49 | 41.58 |  |  | 41.63 |  |  | 41.64 |  | 41.53 | 41.59 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.42 |  |  | 0.02 |  |  |  | 0.85 |  |  |  |  | 0.84 |  |  |  |  |  |  |  | EX |  |  |  | 0.30 | 0.13 |  | 0.85 | 0.63 |  |  | 0.25 |  |  | 0.37 |  | 0.02 | 0.78 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.895 |  |  | 0.883 |  |  |  | 0.905 |  |  |  |  | 0.022 |  |  |  |  | E |  |  | EX |  |  |  | 0.895 | 0.905 |  | 0.904 | 0.902 |  |  | 0.891 |  |  | 0.883 |  | 0.893 | 0.884 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.427 |  |  | 2.413 |  |  |  | 2.441 |  |  |  |  | 0.029 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.422 | 2.432 |  | 2.425 | 2.413 |  |  | 2.425 |  |  | 2.425 |  | 2.441 | 2.436 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.280 |  |  | 3.272 |  |  |  | 3.287 |  |  |  |  | 0.015 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.272 | 3.279 |  | 3.280 | 3.287 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.023 |  |  | 0.017 |  |  |  | 0.029 |  |  |  |  | 0.012 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.187 |  |  | 0.172 |  |  |  | 0.201 |  |  |  |  | 0.029 |  |  |  |  | E |  |  | EX |  |  |  | 0.192 | 0.172 |  | 0.179 | 0.195 |  |  | 0.193 |  |  | 0.201 |  | 0.174 | 0.190 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.180 |  |  | 0.160 |  |  |  | 0.192 |  |  |  |  | 0.031 |  |  |  |  |  |  |  | EX |  |  |  | 0.183 | 0.187 |  | 0.192 | 0.180 |  |  | 0.167 |  |  | 0.181 |  | 0.160 | 0.190 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.086 |  |  | 0.073 |  |  |  | 0.106 |  |  |  |  | 0.033 |  |  |  |  | E |  |  | EX |  |  |  | 0.080 | 0.076 |  | 0.083 | 0.091 |  |  | 0.083 |  |  | 0.099 |  | 0.089 | 0.077 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.084 | 0.086 |  | 0.092 | 0.078 |  |  | 0.073 |  |  | 0.078 |  | 0.094 | 0.106 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 36.15 |  |  | 36.07 |  |  |  | 36.26 |  |  |  |  | 0.20 |  |  |  |  |  |  |  |  |  |  |  | 36.08 | 36.07 |  | 36.26 | 36.19 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.40 |  |  | 40.36 |  |  |  | 40.44 |  |  |  |  | 0.07 |  |  |  |  |  |  |  |  |  |  |  | 40.42 | 40.36 |  | 40.44 | 40.38 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 6.37 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 8.34 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.018 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | 0.29 |  |  |  |  | -0.30 | 0.36 |  |  |  | 0.56 |  |  | 0.24 | 0.44 |  | 0.45 |  |  | Crown, ° |  | -0.19 |  |  |  |  |  |  | EX |  | -1.32 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.30 |  |  | 0.15 |  |  |  |  | 0.55 | 0.99 |  |  |  | 0.31 |  |  | 0.61 | 0.43 |  | 1.23 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.4 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.41 |  |  | -0.36 |  |  |  |  | 0.53 | 0.29 |  |  |  | -0.07 |  |  | 0.12 | -1.32 |  | -0.45 |  |  | Pavilion, ° |  | 0.40 |  |  |  | Digging |  |  | EX |  | 1.10 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.03 |  |  | 0.30 |  |  |  |  | -0.13 | -0.85 |  |  |  | -1.08 |  |  | 0.32 | 0.21 |  | -0.11 |  |  | Pavilion, notch. |  | 0.1, Very small |  |  |  |  |  |  |  |  | 0.3 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | 0.51 |  |  | 0.71 |  |  |  |  | 0.21 | -0.26 |  |  |  | 0.93 |  |  | 0.58 | 0.64 |  | 0.23 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.43 |  |  | 1.10 |  |  |  |  | 0.84 | -0.11 |  |  |  | 0.04 |  |  | 0.61 | 0.10 |  | -0.14 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | V |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.22 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.012 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.25 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.014 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.34 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.019 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.19 %, 0.011 mm |  |  |  |  |  |