| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.854 |  |  | 5.842 |  |  |  | 5.861 |  |  |  |  | 0.33% |  |  |  |  | E |  |  | EX |  |  |  | 5.857 | 5.851 |  | 5.854 | 5.856 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.44 |  |  | 34.29 |  |  |  | 34.51 |  |  |  |  | 0.23 |  |  |  |  | Grading |  |  | EX |  |  |  | 34.40 | 34.39 |  | 34.48 | 34.49 |  |  | 34.47 |  |  | 34.48 |  | 34.29 | 34.51 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.45 |  |  | 41.19 |  |  |  | 41.72 |  |  |  |  | 0.53 |  |  |  |  | Grading |  |  | EX |  |  |  | 41.64 | 41.45 |  | 41.31 | 41.19 |  |  | 41.26 |  |  | 41.41 |  | 41.63 | 41.72 |
| Model |  |  | st5 |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 61.62 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.56 |  |  | 14.40 |  |  |  | 14.69 |  |  |  |  | 0.29 |  |  |  |  | E |  |  | EX |  |  |  | 14.48 | 14.56 |  | 14.69 | 14.69 |  |  | 14.66 |  |  | 14.49 |  | 14.40 | 14.49 |
| Report date |  |  | 11.12.2007 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 43.97 |  |  | 43.83 |  |  |  | 44.16 |  |  |  |  | 0.33 |  |  |  |  | N/A |  |  | EX |  |  |  | 43.89 | 43.83 |  | 43.95 | 43.87 |  |  | 44.00 |  |  | 43.97 |  | 44.16 | 44.13 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.57 |  |  | 57.53 |  |  |  | 57.60 |  |  |  |  | 0.07 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.53 | 57.56 |  | 57.60 | 57.58 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.75, 0.7502 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.36 |  |  | 0.27 |  |  |  | 0.43 |  |  |  |  | 0.17 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.854 (5.842-5.861) x 3.607 /0.009 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 3.08 |  |  | 2.91 |  |  |  | 3.29 |  |  |  |  | 0.38 |  |  |  |  | E |  |  | EX |  |  |  | 3.29 | 3.22 |  | 2.93 | 3.07 |  |  | 2.91 |  |  | 3.16 |  | 3.08 | 3.00 |
| Spread |  |  | -0.01 ct, -0.95% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 3.16 |  |  | 3.02 |  |  |  | 3.39 |  |  |  |  | 0.38 |  |  |  |  |  |  |  | EX |  |  |  | 3.23 | 3.04 |  | 3.39 | 3.17 |  |  | 3.26 |  |  | 3.09 |  | 3.07 | 3.02 |
| AGS Spread |  |  | -0.01 ct, -1.27% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.51 |  |  | 1.29 |  |  |  | 1.88 |  |  |  |  | 0.59 |  |  |  |  | E |  |  | EX |  |  |  | 1.64 | 1.88 |  | 1.43 | 1.43 |  |  | 1.40 |  |  | 1.75 |  | 1.36 | 1.40 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.48 | 1.46 |  | 1.73 | 1.38 |  |  | 1.55 |  |  | 1.32 |  | 1.29 | 1.67 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 52.90: |  |  | 52.01: |  |  |  | 54.23: |  |  |  |  | 2.22 |  |  |  |  | E |  |  | VG |  |  |  | 52.75: | 52.01: |  | 52.43: | 52.24: |  |  | 53.37: |  |  | 52.64: |  | 54.23: | 53.56: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 47.10 |  |  | 47.99 |  |  |  | 45.77 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 47.25 | 47.99 |  | 47.57 | 47.76 |  |  | 46.63 |  |  | 47.36 |  | 45.77 | 46.44 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 22.22 |  |  | 22.08 |  |  |  | 22.31 |  |  |  |  | 0.24 |  |  |  |  |  |  |  | EX |  |  |  | 22.24 | 22.20 |  | 22.28 | 22.17 |  |  | 22.08 |  |  | 22.31 |  | 22.15 | 22.30 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 41.26 |  |  | 40.65 |  |  |  | 41.49 |  |  |  |  | 0.84 |  |  |  |  |  |  |  | EX |  |  |  | 41.28 | 41.28 |  | 41.09 | 41.46 |  |  | 41.03 |  |  | 41.35 |  | 41.18 | 41.30 |
| 5.854 | 3.607 | 0.852 | 2.574 | 3.370 |  | 0.021 | 0.180 | 0.185 | 0.088 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.06 | 41.49 |  | 40.65 | 41.37 |  |  | 41.24 |  |  | 41.44 |  | 41.45 | 41.43 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 80.54 |  |  | 79.66 |  |  |  | 81.58 |  |  |  |  | 1.91 |  |  |  |  | E |  |  | EX |  |  |  | 80.28 | 79.82 |  | 80.60 | 80.53 |  |  | 79.89 |  |  | 80.64 |  | 81.03 | 81.17 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 81.09 | 81.58 |  | 81.18 | 81.16 |  |  | 79.97 |  |  | 80.10 |  | 79.66 | 79.98 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.51 |  |  | 42.25 |  |  |  | 42.85 |  |  |  |  | 0.60 |  |  |  |  |  |  |  | EX |  |  |  | 42.67 | 42.52 |  | 42.50 | 42.40 |  |  | 42.35 |  |  | 42.25 |  | 42.25 | 42.25 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.27 | 42.37 |  | 42.54 | 42.65 |  |  | 42.71 |  |  | 42.77 |  | 42.85 | 42.75 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.67 |  |  | 0.27 |  |  |  | 1.11 |  |  |  |  | 0.84 |  |  |  |  |  |  |  | EX |  |  |  | 0.95 | 0.99 |  | 1.11 | 0.34 |  |  | 0.37 |  |  | 0.37 |  | 0.27 | 1.00 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.852 |  |  | 0.843 |  |  |  | 0.860 |  |  |  |  | 0.017 |  |  |  |  | E |  |  | EX |  |  |  | 0.847 | 0.852 |  | 0.860 | 0.860 |  |  | 0.858 |  |  | 0.848 |  | 0.843 | 0.848 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.574 |  |  | 2.566 |  |  |  | 2.585 |  |  |  |  | 0.019 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.569 | 2.566 |  | 2.573 | 2.568 |  |  | 2.576 |  |  | 2.574 |  | 2.585 | 2.583 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.370 |  |  | 3.368 |  |  |  | 3.372 |  |  |  |  | 0.004 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.368 | 3.370 |  | 3.372 | 3.370 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.021 |  |  | 0.016 |  |  |  | 0.025 |  |  |  |  | 0.010 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.180 |  |  | 0.170 |  |  |  | 0.192 |  |  |  |  | 0.022 |  |  |  |  | E |  |  | EX |  |  |  | 0.192 | 0.188 |  | 0.172 | 0.180 |  |  | 0.170 |  |  | 0.185 |  | 0.180 | 0.176 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.185 |  |  | 0.177 |  |  |  | 0.199 |  |  |  |  | 0.022 |  |  |  |  |  |  |  | EX |  |  |  | 0.189 | 0.178 |  | 0.199 | 0.186 |  |  | 0.191 |  |  | 0.181 |  | 0.180 | 0.177 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.088 |  |  | 0.076 |  |  |  | 0.110 |  |  |  |  | 0.034 |  |  |  |  | E |  |  | EX |  |  |  | 0.096 | 0.110 |  | 0.084 | 0.084 |  |  | 0.082 |  |  | 0.103 |  | 0.079 | 0.082 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.087 | 0.086 |  | 0.101 | 0.081 |  |  | 0.091 |  |  | 0.077 |  | 0.076 | 0.098 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.44 |  |  | 34.38 |  |  |  | 34.50 |  |  |  |  | 0.12 |  |  |  |  |  |  |  |  |  |  |  | 34.44 | 34.43 |  | 34.38 | 34.50 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.45 |  |  | 41.43 |  |  |  | 41.47 |  |  |  |  | 0.04 |  |  |  |  |  |  |  |  |  |  |  | 41.45 | 41.43 |  | 41.47 | 41.45 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 10.54 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 11.12 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.009 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | -0.14 |  |  |  |  | -0.12 | 0.12 |  |  |  | -0.23 |  |  | 0.30 | -0.09 |  | 0.21 |  |  | Crown, ° |  | -0.44 |  |  |  | Painting |  |  | EX |  | -1.70 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.95 |  |  | 0.86 |  |  |  |  | 0.99 | 0.46 |  |  |  | 0.14 |  |  | 0.68 | 0.17 |  | 1.21 |  |  | Crown, notch. |  | 0.1, Very small |  |  |  |  |  |  |  |  | 0.5 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.56 |  |  | 0.52 |  |  |  |  | -1.26 | 0.75 |  |  |  | -1.35 |  |  | 0.10 | -0.67 |  | 0.43 |  |  | Pavilion, ° |  | -0.01 |  |  |  |  |  |  | EX |  | 0.28 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -1.20 |  |  | 0.18 |  |  |  |  | -1.70 | -0.32 |  |  |  | -0.65 |  |  | -0.35 | -0.97 |  | 0.02 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.1 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | 0.10 |  |  | -0.27 |  |  |  |  | 0.10 | -0.21 |  |  |  | 0.09 |  |  | 0.04 | 0.02 |  | -0.23 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.28 |  |  | 0.22 |  |  |  |  | -0.18 | -0.17 |  |  |  | 0.02 |  |  | 0.22 | -0.18 |  | -0.08 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.37 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.022 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.13 ± 0.19, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.007 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.35 ± 0.23, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.020 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.16 %, 0.009 mm |  |  |  |  |  |