| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.808 |  |  | 5.798 |  |  |  | 5.815 |  |  |  |  | 0.30% |  |  |  |  | E |  |  | EX |  |  |  | 5.812 | 5.806 |  | 5.814 | 5.813 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.47 |  |  | 34.31 |  |  |  | 34.66 |  |  |  |  | 0.35 |  |  |  |  | Grading |  |  | EX |  |  |  | 34.34 | 34.31 |  | 34.42 | 34.49 |  |  | 34.66 |  |  | 34.65 |  | 34.49 | 34.38 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.61 |  |  | 41.51 |  |  |  | 41.77 |  |  |  |  | 0.26 |  |  |  |  | Grading |  |  | EX |  |  |  | 41.77 | 41.60 |  | 41.56 | 41.51 |  |  | 41.51 |  |  | 41.56 |  | 41.65 | 41.73 |
| Model |  |  | st6 |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 61.60 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.56 |  |  | 14.34 |  |  |  | 14.76 |  |  |  |  | 0.41 |  |  |  |  | E |  |  | EX |  |  |  | 14.34 | 14.48 |  | 14.51 | 14.66 |  |  | 14.67 |  |  | 14.76 |  | 14.59 | 14.50 |
| Report date |  |  | 11.12.2007 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 44.25 |  |  | 43.90 |  |  |  | 44.61 |  |  |  |  | 0.72 |  |  |  |  | N/A |  |  | VG |  |  |  | 44.61 | 44.51 |  | 44.26 | 44.08 |  |  | 43.96 |  |  | 43.90 |  | 44.16 | 44.51 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.71 |  |  | 57.50 |  |  |  | 58.00 |  |  |  |  | 0.50 |  |  |  |  | Grading |  |  | EX |  |  |  | 58.00 | 57.50 |  | 57.68 | 57.64 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.72, 0.7275 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.33 |  |  | 0.30 |  |  |  | 0.36 |  |  |  |  | 0.06 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.808 (5.798-5.815) x 3.578 /0.005 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 2.78 |  |  | 2.59 |  |  |  | 2.97 |  |  |  |  | 0.38 |  |  |  |  | E |  |  | EX |  |  |  | 2.61 | 2.62 |  | 2.83 | 2.82 |  |  | 2.97 |  |  | 2.95 |  | 2.83 | 2.59 |
| Spread |  |  | 0.01 ct, 0.77% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 2.87 |  |  | 2.78 |  |  |  | 3.01 |  |  |  |  | 0.23 |  |  |  |  |  |  |  | EX |  |  |  | 2.82 | 2.87 |  | 2.78 | 2.95 |  |  | 3.01 |  |  | 2.79 |  | 2.83 | 2.91 |
| AGS Spread |  |  | 0.00 ct, 0.45% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.13 |  |  | 0.95 |  |  |  | 1.34 |  |  |  |  | 0.39 |  |  |  |  | E |  |  | EX |  |  |  | 1.02 | 0.95 |  | 1.00 | 1.02 |  |  | 1.20 |  |  | 1.13 |  | 1.26 | 1.19 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.34 | 1.28 |  | 1.08 | 1.13 |  |  | 1.21 |  |  | 1.03 |  | 1.11 | 1.05 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 53.27: |  |  | 52.03: |  |  |  | 54.73: |  |  |  |  | 2.70 |  |  |  |  | E |  |  | VG |  |  |  | 53.33: | 53.59: |  | 52.03: | 52.91: |  |  | 52.89: |  |  | 53.11: |  | 53.58: | 54.73: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 46.73 |  |  | 47.97 |  |  |  | 45.27 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 46.67 | 46.41 |  | 47.97 | 47.09 |  |  | 47.11 |  |  | 46.89 |  | 46.42 | 45.27 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 22.23 |  |  | 22.00 |  |  |  | 22.56 |  |  |  |  | 0.56 |  |  |  |  |  |  |  | EX |  |  |  | 22.13 | 22.11 |  | 22.28 | 22.00 |  |  | 22.09 |  |  | 22.19 |  | 22.56 | 22.46 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 41.74 |  |  | 41.36 |  |  |  | 42.31 |  |  |  |  | 0.94 |  |  |  |  |  |  |  | EX |  |  |  | 41.83 | 41.41 |  | 42.11 | 41.55 |  |  | 42.04 |  |  | 41.38 |  | 42.13 | 42.31 |
| 5.808 | 3.578 | 0.846 | 2.570 | 3.351 |  | 0.019 | 0.161 | 0.167 | 0.065 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.16 | 41.97 |  | 41.59 | 41.53 |  |  | 41.37 |  |  | 41.36 |  | 41.53 | 41.53 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 80.56 |  |  | 78.98 |  |  |  | 81.40 |  |  |  |  | 2.42 |  |  |  |  | E |  |  | EX |  |  |  | 81.40 | 80.51 |  | 80.25 | 80.38 |  |  | 80.46 |  |  | 80.53 |  | 80.62 | 81.24 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 80.92 | 80.48 |  | 80.73 | 80.36 |  |  | 80.51 |  |  | 80.72 |  | 78.98 | 80.93 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.66 |  |  | 42.53 |  |  |  | 42.80 |  |  |  |  | 0.27 |  |  |  |  |  |  |  | EX |  |  |  | 42.74 | 42.76 |  | 42.65 | 42.59 |  |  | 42.62 |  |  | 42.60 |  | 42.54 | 42.59 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.55 | 42.53 |  | 42.72 | 42.71 |  |  | 42.74 |  |  | 42.80 |  | 42.72 | 42.76 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.61 |  |  | 0.22 |  |  |  | 1.24 |  |  |  |  | 1.02 |  |  |  |  |  |  |  | VG |  |  |  | 0.68 | 0.58 |  | 0.54 | 1.24 |  |  | 0.22 |  |  | 0.53 |  | 0.24 | 0.88 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.846 |  |  | 0.833 |  |  |  | 0.857 |  |  |  |  | 0.024 |  |  |  |  | E |  |  | EX |  |  |  | 0.833 | 0.841 |  | 0.843 | 0.851 |  |  | 0.852 |  |  | 0.857 |  | 0.848 | 0.842 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.570 |  |  | 2.549 |  |  |  | 2.591 |  |  |  |  | 0.042 |  |  |  |  | N/A |  |  | VG |  |  |  | 2.591 | 2.585 |  | 2.570 | 2.560 |  |  | 2.553 |  |  | 2.549 |  | 2.565 | 2.585 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.351 |  |  | 3.339 |  |  |  | 3.369 |  |  |  |  | 0.029 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.369 | 3.339 |  | 3.350 | 3.348 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.019 |  |  | 0.017 |  |  |  | 0.021 |  |  |  |  | 0.004 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.161 |  |  | 0.151 |  |  |  | 0.173 |  |  |  |  | 0.022 |  |  |  |  | E |  |  | EX |  |  |  | 0.151 | 0.152 |  | 0.165 | 0.164 |  |  | 0.173 |  |  | 0.171 |  | 0.164 | 0.151 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.167 |  |  | 0.162 |  |  |  | 0.175 |  |  |  |  | 0.013 |  |  |  |  |  |  |  | EX |  |  |  | 0.164 | 0.167 |  | 0.162 | 0.171 |  |  | 0.175 |  |  | 0.162 |  | 0.165 | 0.169 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.065 |  |  | 0.055 |  |  |  | 0.078 |  |  |  |  | 0.023 |  |  |  |  | E |  |  | EX |  |  |  | 0.059 | 0.055 |  | 0.058 | 0.059 |  |  | 0.070 |  |  | 0.066 |  | 0.073 | 0.069 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.078 | 0.074 |  | 0.063 | 0.066 |  |  | 0.070 |  |  | 0.060 |  | 0.065 | 0.061 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.47 |  |  | 34.43 |  |  |  | 34.50 |  |  |  |  | 0.07 |  |  |  |  |  |  |  |  |  |  |  | 34.50 | 34.48 |  | 34.46 | 34.43 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 41.61 |  |  | 41.58 |  |  |  | 41.64 |  |  |  |  | 0.06 |  |  |  |  |  |  |  |  |  |  |  | 41.64 | 41.58 |  | 41.61 | 41.62 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 11.17 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 11.23 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.005 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | -0.17 |  |  |  |  | -0.19 | -0.07 |  |  |  | -0.27 |  |  | -0.21 | -0.08 |  | 0.38 |  |  | Crown, ° |  | -0.01 |  |  |  |  |  |  | EX |  | 1.17 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | -0.68 |  |  | -0.75 |  |  |  |  | -0.74 | -1.32 |  |  |  | -0.49 |  |  | 0.32 | -0.32 |  | -0.50 |  |  | Crown, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.3 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | 0.51 |  |  | -0.21 |  |  |  |  | 0.96 | -0.34 |  |  |  | 0.99 |  |  | -0.70 | 1.17 |  | 0.19 |  |  | Pavilion, ° |  | -0.10 |  |  |  |  |  |  | EX |  | -0.74 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.56 |  |  | 0.05 |  |  |  |  | -1.03 | 0.31 |  |  |  | -0.88 |  |  | -0.61 | -0.40 |  | -0.71 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.2 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | -0.50 |  |  | 0.49 |  |  |  |  | -0.56 | -0.20 |  |  |  | -0.15 |  |  | 0.27 | -0.23 |  | 0.21 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.18 |  |  | -0.31 |  |  |  |  | 0.18 | -0.03 |  |  |  | 0.22 |  |  | 0.02 | -0.74 |  | -0.43 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.19 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.011 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.13 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.008 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.32 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.019 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.06 %, 0.003 mm |  |  |  |  |  |