| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.770 |  |  | 5.764 |  |  |  | 5.776 |  |  |  |  | 0.22% |  |  |  |  | E |  |  | EX |  |  |  | 5.772 | 5.776 |  | 5.772 | 5.772 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.55 |  |  | 34.36 |  |  |  | 34.83 |  |  |  |  | 0.47 |  |  |  |  | Grading |  |  | EX |  |  |  | 34.68 | 34.75 |  | 34.83 | 34.59 |  |  | 34.38 |  |  | 34.36 |  | 34.36 | 34.47 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.16 |  |  | 39.97 |  |  |  | 40.32 |  |  |  |  | 0.35 |  |  |  |  | Grading |  |  | EX |  |  |  | 40.10 | 39.97 |  | 39.98 | 40.17 |  |  | 40.32 |  |  | 40.25 |  | 40.31 | 40.16 |
| Model |  |  | st8 |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 59.84 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.75 |  |  | 14.54 |  |  |  | 14.91 |  |  |  |  | 0.37 |  |  |  |  | E |  |  | EX |  |  |  | 14.79 | 14.86 |  | 14.91 | 14.84 |  |  | 14.68 |  |  | 14.63 |  | 14.54 | 14.74 |
| Report date |  |  | 11.12.2007 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 42.07 |  |  | 41.84 |  |  |  | 42.25 |  |  |  |  | 0.41 |  |  |  |  | N/A |  |  | EX |  |  |  | 42.05 | 41.94 |  | 41.84 | 42.04 |  |  | 42.22 |  |  | 42.15 |  | 42.25 | 42.07 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.30 |  |  | 57.14 |  |  |  | 57.47 |  |  |  |  | 0.33 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.24 | 57.37 |  | 57.47 | 57.14 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.70, 0.7031 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.37 |  |  | 0.33 |  |  |  | 0.40 |  |  |  |  | 0.07 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.770 (5.764-5.776) x 3.453 /0.001 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 3.01 |  |  | 2.94 |  |  |  | 3.09 |  |  |  |  | 0.14 |  |  |  |  | E |  |  | EX |  |  |  | 2.97 | 3.04 |  | 3.09 | 2.96 |  |  | 2.94 |  |  | 3.04 |  | 3.05 | 3.01 |
| Spread |  |  | 0.01 ct, 1.65% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 2.89 |  |  | 2.59 |  |  |  | 3.15 |  |  |  |  | 0.56 |  |  |  |  |  |  |  | EX |  |  |  | 2.85 | 3.15 |  | 2.92 | 2.66 |  |  | 2.99 |  |  | 2.92 |  | 3.01 | 2.59 |
| AGS Spread |  |  | 0.01 ct, 1.32% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.33 |  |  | 1.05 |  |  |  | 1.58 |  |  |  |  | 0.53 |  |  |  |  | E |  |  | EX |  |  |  | 1.14 | 1.39 |  | 1.55 | 1.58 |  |  | 1.26 |  |  | 1.25 |  | 1.05 | 1.21 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.26 | 1.37 |  | 1.50 | 1.27 |  |  | 1.53 |  |  | 1.49 |  | 1.24 | 1.14 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 53.61: |  |  | 52.75: |  |  |  | 54.54: |  |  |  |  | 1.79 |  |  |  |  | E |  |  | EX |  |  |  | 54.17: | 53.80: |  | 53.41: | 54.54: |  |  | 53.18: |  |  | 53.60: |  | 53.44: | 52.75: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 46.39 |  |  | 47.25 |  |  |  | 45.46 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 45.83 | 46.20 |  | 46.59 | 45.46 |  |  | 46.82 |  |  | 46.40 |  | 46.56 | 47.25 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 22.31 |  |  | 21.99 |  |  |  | 22.67 |  |  |  |  | 0.67 |  |  |  |  |  |  |  | EX |  |  |  | 22.34 | 22.48 |  | 22.67 | 22.43 |  |  | 21.99 |  |  | 22.23 |  | 22.30 | 22.07 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 42.00 |  |  | 41.46 |  |  |  | 42.40 |  |  |  |  | 0.94 |  |  |  |  |  |  |  | EX |  |  |  | 42.12 | 41.94 |  | 42.16 | 42.31 |  |  | 42.05 |  |  | 42.01 |  | 42.40 | 42.08 |
| 5.770 | 3.453 | 0.851 | 2.428 | 3.307 |  | 0.021 | 0.174 | 0.167 | 0.076 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.72 | 41.46 |  | 41.79 | 41.79 |  |  | 42.00 |  |  | 42.03 |  | 41.80 | 42.40 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 78.02 |  |  | 77.23 |  |  |  | 78.67 |  |  |  |  | 1.44 |  |  |  |  | E |  |  | EX |  |  |  | 78.09 | 77.83 |  | 78.46 | 78.57 |  |  | 78.67 |  |  | 78.67 |  | 77.87 | 78.00 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 77.23 | 78.13 |  | 78.14 | 78.03 |  |  | 77.32 |  |  | 77.45 |  | 77.66 | 78.22 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 41.37 |  |  | 41.05 |  |  |  | 41.52 |  |  |  |  | 0.47 |  |  |  |  |  |  |  | EX |  |  |  | 41.49 | 41.32 |  | 41.05 | 41.06 |  |  | 41.25 |  |  | 41.30 |  | 41.47 | 41.51 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 41.48 | 41.50 |  | 41.48 | 41.52 |  |  | 41.40 |  |  | 41.30 |  | 41.38 | 41.38 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.49 |  |  | 0.17 |  |  |  | 0.89 |  |  |  |  | 0.72 |  |  |  |  |  |  |  | EX |  |  |  | 0.89 | 0.47 |  | 0.17 | 0.61 |  |  | 0.49 |  |  | 0.25 |  | 0.32 | 0.73 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.851 |  |  | 0.839 |  |  |  | 0.860 |  |  |  |  | 0.021 |  |  |  |  | E |  |  | EX |  |  |  | 0.853 | 0.858 |  | 0.860 | 0.856 |  |  | 0.847 |  |  | 0.844 |  | 0.839 | 0.851 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.428 |  |  | 2.414 |  |  |  | 2.438 |  |  |  |  | 0.024 |  |  |  |  | N/A |  |  | EX |  |  |  | 2.427 | 2.420 |  | 2.414 | 2.426 |  |  | 2.436 |  |  | 2.432 |  | 2.438 | 2.427 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.307 |  |  | 3.297 |  |  |  | 3.316 |  |  |  |  | 0.019 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.303 | 3.310 |  | 3.316 | 3.297 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.021 |  |  | 0.019 |  |  |  | 0.023 |  |  |  |  | 0.004 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.174 |  |  | 0.170 |  |  |  | 0.178 |  |  |  |  | 0.008 |  |  |  |  | E |  |  | EX |  |  |  | 0.172 | 0.175 |  | 0.178 | 0.171 |  |  | 0.170 |  |  | 0.176 |  | 0.176 | 0.174 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.167 |  |  | 0.149 |  |  |  | 0.182 |  |  |  |  | 0.032 |  |  |  |  |  |  |  | EX |  |  |  | 0.165 | 0.182 |  | 0.169 | 0.154 |  |  | 0.173 |  |  | 0.169 |  | 0.174 | 0.149 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.076 |  |  | 0.061 |  |  |  | 0.091 |  |  |  |  | 0.030 |  |  |  |  | E |  |  | EX |  |  |  | 0.066 | 0.080 |  | 0.089 | 0.091 |  |  | 0.073 |  |  | 0.072 |  | 0.061 | 0.070 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.072 | 0.079 |  | 0.086 | 0.073 |  |  | 0.088 |  |  | 0.086 |  | 0.071 | 0.066 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.55 |  |  | 34.53 |  |  |  | 34.60 |  |  |  |  | 0.07 |  |  |  |  |  |  |  |  |  |  |  | 34.53 | 34.55 |  | 34.60 | 34.53 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.16 |  |  | 40.11 |  |  |  | 40.21 |  |  |  |  | 0.10 |  |  |  |  |  |  |  |  |  |  |  | 40.21 | 40.11 |  | 40.15 | 40.17 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 5.42 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 12.36 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.001 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | 0.66 |  |  |  |  | 0.64 | 0.87 |  |  |  | 0.77 |  |  | 1.05 | 0.58 |  | 0.11 |  |  | Crown, ° |  | 0.25 |  |  |  |  |  |  | EX |  | 1.25 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 0.89 |  |  | 1.12 |  |  |  |  | 0.81 | 0.26 |  |  |  | 0.28 |  |  | 0.80 | 0.90 |  | 0.85 |  |  | Crown, notch. |  | 0.1, Negligible |  |  |  |  |  |  |  |  | 0.3 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -0.13 |  |  | -0.24 |  |  |  |  | 0.28 | 0.40 |  |  |  | -0.34 |  |  | -0.07 | 0.76 |  | 0.13 |  |  | Pavilion, ° |  | 0.34 |  |  |  |  |  |  | EX |  | 1.28 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.41 |  |  | -0.60 |  |  |  |  | 0.70 | -0.08 |  |  |  | 0.92 |  |  | 0.64 | 0.00 |  | 1.25 |  |  | Pavilion, notch. |  | 0.1, Negligible |  |  |  |  |  |  |  |  | 0.3 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | 1.28 |  |  | 0.60 |  |  |  |  | 0.14 | 0.24 |  |  |  | 0.31 |  |  | 0.39 | 0.49 |  | 0.25 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.01 |  |  | 0.50 |  |  |  |  | 0.68 | -0.30 |  |  |  | -0.02 |  |  | 0.02 | 0.27 |  | 0.61 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | V |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.10 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.006 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.06 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.004 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.07 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.004 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.07 %, 0.004 mm |  |  |  |  |  |