| # ILLUSTRATED REPORT FOR BRILLIANT |  |  |  |  |  |  |  |  |  |  |  |  | Parameter |  |  | Avg |  |  | Min |  |  |  | Max |  |  |  |  | Dev |  |  |  |  | Cut |  |  | Sym |  |  |  | 1 | 2 |  | 3 | 4 |  |  | 5 |  |  | 6 |  | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  |  |  |  |  |  |  |  |  |  | Diameter, mm |  |  | 5.775 |  |  | 5.765 |  |  |  | 5.783 |  |  |  |  | 0.31% |  |  |  |  | E |  |  | EX |  |  |  | 5.777 | 5.782 |  | 5.774 | 5.772 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.48 |  |  | 34.34 |  |  |  | 34.56 |  |  |  |  | 0.22 |  |  |  |  | Grading |  |  | EX |  |  |  | 34.56 | 34.52 |  | 34.54 | 34.41 |  |  | 34.46 |  |  | 34.48 |  | 34.34 | 34.54 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.94 |  |  | 40.75 |  |  |  | 41.05 |  |  |  |  | 0.30 |  |  |  |  | Grading |  |  | EX |  |  |  | 40.86 | 40.80 |  | 40.75 | 40.97 |  |  | 41.02 |  |  | 41.05 |  | 41.05 | 41.01 |
| Model |  |  | st9 |  |  |  |  |  |  |  |  |  | Total height, % |  |  | 60.80 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Expert name |  |  | Makoed A.G. |  |  |  |  |  |  |  |  |  | Crown height, % |  |  | 14.63 |  |  | 14.40 |  |  |  | 14.89 |  |  |  |  | 0.49 |  |  |  |  | E |  |  | EX |  |  |  | 14.45 | 14.60 |  | 14.89 | 14.79 |  |  | 14.74 |  |  | 14.69 |  | 14.40 | 14.45 |
| Report date |  |  | 12.12.2007 |  |  |  |  |  |  |  |  |  | Pavilion depth, % |  |  | 43.22 |  |  | 42.88 |  |  |  | 43.64 |  |  |  |  | 0.75 |  |  |  |  | N/A |  |  | VG |  |  |  | 43.58 | 43.28 |  | 42.88 | 42.98 |  |  | 42.95 |  |  | 43.09 |  | 43.36 | 43.64 |
| Real weight, ct |  |  |  |  |  |  |  |  |  |  |  |  | Table, % |  |  | 57.46 |  |  | 57.29 |  |  |  | 57.57 |  |  |  |  | 0.28 |  |  |  |  | Grading |  |  | EX |  |  |  | 57.56 | 57.57 |  | 57.29 | 57.40 |  |  |  |  |  |  |  |  |  |
| Calculated weight, ct |  |  | 0.71, 0.7120 |  |  |  |  |  |  |  |  |  | Culet, % |  |  | 0.37 |  |  | 0.28 |  |  |  | 0.44 |  |  |  |  | 0.16 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Measurements |  |  | 5.775 (5.765-5.783) x 3.511 /0.004 mm |  |  |  |  |  |  |  |  |  | Girdle Bezel, % |  |  | 2.95 |  |  | 2.72 |  |  |  | 3.11 |  |  |  |  | 0.39 |  |  |  |  | E |  |  | EX |  |  |  | 2.77 | 2.92 |  | 2.98 | 3.03 |  |  | 3.11 |  |  | 3.02 |  | 3.05 | 2.72 |
| Spread |  |  | 0.00 ct, 0.49% |  |  |  |  |  |  |  |  |  | Girdle Bone, % |  |  | 3.23 |  |  | 3.03 |  |  |  | 3.32 |  |  |  |  | 0.30 |  |  |  |  |  |  |  | EX |  |  |  | 3.23 | 3.21 |  | 3.03 | 3.27 |  |  | 3.29 |  |  | 3.24 |  | 3.22 | 3.32 |
| AGS Spread |  |  | 0.00 ct, 0.17% |  |  |  |  |  |  |  |  |  | Girdle Valley, % |  |  | 1.44 |  |  | 1.14 |  |  |  | 1.66 |  |  |  |  | 0.53 |  |  |  |  | E |  |  | EX |  |  |  | 1.34 | 1.51 |  | 1.52 | 1.46 |  |  | 1.41 |  |  | 1.36 |  | 1.50 | 1.28 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.55 | 1.66 |  | 1.49 | 1.50 |  |  | 1.42 |  |  | 1.14 |  | 1.39 | 1.55 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  |  | Star: |  |  | 53.76: |  |  | 52.77: |  |  |  | 54.91: |  |  |  |  | 2.14 |  |  |  |  | E |  |  | VG |  |  |  | 53.51: | 52.77: |  | 53.14: | 53.24: |  |  | 53.86: |  |  | 54.33: |  | 54.30: | 54.91: |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Upper ratio, % |  |  | 46.24 |  |  | 47.23 |  |  |  | 45.09 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 46.49 | 47.23 |  | 46.86 | 46.76 |  |  | 46.14 |  |  | 45.67 |  | 45.70 | 45.09 |
| Diam | Total height | Crown height | Pav. depth | Table |  | Culet | Girdle |  |  |  |  |  | Star angle, ° |  |  | 22.41 |  |  | 22.18 |  |  |  | 22.69 |  |  |  |  | 0.51 |  |  |  |  |  |  |  | EX |  |  |  | 22.25 | 22.42 |  | 22.55 | 22.38 |  |  | 22.53 |  |  | 22.69 |  | 22.18 | 22.28 |
|  |  |  |  |  |  |  | Bezel | Bone | Valley |  |  |  | Upper girdle angle, ° |  |  | 41.01 |  |  | 40.70 |  |  |  | 41.35 |  |  |  |  | 0.65 |  |  |  |  |  |  |  | EX |  |  |  | 41.09 | 41.19 |  | 41.35 | 41.01 |  |  | 40.88 |  |  | 41.21 |  | 40.84 | 40.70 |
| 5.775 | 3.511 | 0.845 | 2.496 | 3.318 |  | 0.021 | 0.170 | 0.186 | 0.083 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 40.93 | 40.97 |  | 41.04 | 41.26 |  |  | 40.85 |  |  | 40.97 |  | 40.96 | 40.95 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % |  |  | 79.72 |  |  | 79.21 |  |  |  | 80.75 |  |  |  |  | 1.54 |  |  |  |  | E |  |  | EX |  |  |  | 80.75 | 80.20 |  | 79.78 | 79.65 |  |  | 79.28 |  |  | 79.52 |  | 79.46 | 79.99 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 79.48 | 79.99 |  | 79.21 | 80.03 |  |  | 79.64 |  |  | 79.60 |  | 79.40 | 79.64 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Lower girdle angle / Halves angle, ° |  |  | 42.03 |  |  | 41.84 |  |  |  | 42.17 |  |  |  |  | 0.33 |  |  |  |  |  |  |  | EX |  |  |  | 41.91 | 41.89 |  | 41.84 | 41.84 |  |  | 41.84 |  |  | 42.07 |  | 42.10 | 42.11 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 42.15 | 42.09 |  | 42.11 | 42.11 |  |  | 42.17 |  |  | 42.17 |  | 42.08 | 42.01 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Twist, ° |  |  | 0.47 |  |  | 0.05 |  |  |  | 1.01 |  |  |  |  | 0.96 |  |  |  |  |  |  |  | EX |  |  |  | 1.01 | 1.00 |  | 0.57 | 0.24 |  |  | 0.18 |  |  | 0.05 |  | 0.47 | 0.20 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown height, mm |  |  | 0.845 |  |  | 0.831 |  |  |  | 0.860 |  |  |  |  | 0.029 |  |  |  |  | E |  |  | EX |  |  |  | 0.834 | 0.843 |  | 0.860 | 0.854 |  |  | 0.851 |  |  | 0.849 |  | 0.831 | 0.834 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion depth, mm |  |  | 2.496 |  |  | 2.477 |  |  |  | 2.520 |  |  |  |  | 0.044 |  |  |  |  | N/A |  |  | VG |  |  |  | 2.517 | 2.500 |  | 2.477 | 2.482 |  |  | 2.481 |  |  | 2.489 |  | 2.504 | 2.520 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table, mm |  |  | 3.318 |  |  | 3.309 |  |  |  | 3.325 |  |  |  |  | 0.016 |  |  |  |  | Grading |  |  | EX |  |  |  | 3.324 | 3.325 |  | 3.309 | 3.315 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet, mm |  |  | 0.021 |  |  | 0.016 |  |  |  | 0.025 |  |  |  |  | 0.009 |  |  |  |  | E |  |  | EX |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bezel, mm |  |  | 0.170 |  |  | 0.157 |  |  |  | 0.179 |  |  |  |  | 0.022 |  |  |  |  | E |  |  | EX |  |  |  | 0.160 | 0.169 |  | 0.172 | 0.175 |  |  | 0.179 |  |  | 0.174 |  | 0.176 | 0.157 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Bone, mm |  |  | 0.186 |  |  | 0.175 |  |  |  | 0.192 |  |  |  |  | 0.017 |  |  |  |  |  |  |  | EX |  |  |  | 0.187 | 0.185 |  | 0.175 | 0.189 |  |  | 0.190 |  |  | 0.187 |  | 0.186 | 0.192 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle Valley, mm |  |  | 0.083 |  |  | 0.066 |  |  |  | 0.096 |  |  |  |  | 0.030 |  |  |  |  | E |  |  | EX |  |  |  | 0.078 | 0.087 |  | 0.088 | 0.084 |  |  | 0.081 |  |  | 0.078 |  | 0.087 | 0.074 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.089 | 0.096 |  | 0.086 | 0.086 |  |  | 0.082 |  |  | 0.066 |  | 0.081 | 0.090 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Measurement as per OctoNus theory: |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown angle, ° |  |  | 34.48 |  |  | 34.44 |  |  |  | 34.51 |  |  |  |  | 0.07 |  |  |  |  |  |  |  |  |  |  |  | 34.51 | 34.50 |  | 34.44 | 34.48 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion angle, ° |  |  | 40.94 |  |  | 40.90 |  |  |  | 40.99 |  |  |  |  | 0.09 |  |  |  |  |  |  |  |  |  |  |  | 40.94 | 40.93 |  | 40.90 | 40.99 |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Fish eye effect, ° |  |  |  |  |  |  |  |  |  |  | 8.52 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Extra Facet / Nat |  |  |  |  | No |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Culet through Crown Bezel, ° |  |  |  |  |  |  |  |  |  |  | 11.72 |  |  |  |  |  |  |  |  | N/A |  |  |  |  |  |  | Girdle to MIC, mm |  |  |  |  | 0.004 |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Parameter, ° |  |  |  |  | 1 |  |  | 2 |  |  |  |  | 3 | 4 |  |  |  | 5 |  |  | 6 | 7 |  | 8 |  |  | Paint / Dug |  | Avg |  |  |  | Type |  |  | Sym |  | Dev |  | Sym |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pav. azimuths dev. from ideal |  |  |  |  | 0.00 |  |  | 0.31 |  |  |  |  | 0.65 | 0.66 |  |  |  | 0.68 |  |  | 0.50 | 0.47 |  | 0.01 |  |  | Crown, ° |  | -0.91 |  |  |  | Painting |  |  | EX |  | -1.35 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown azimuths dev. from ideal |  |  |  |  | 1.01 |  |  | 1.32 |  |  |  |  | 1.22 | 0.42 |  |  |  | 0.50 |  |  | 0.56 | 0.01 |  | 0.21 |  |  | Crown, notch. |  | 0.2, Very small |  |  |  |  |  |  |  |  | 0.4 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Crown painting |  |  |  |  | -1.14 |  |  | -0.88 |  |  |  |  | -0.21 | -0.88 |  |  |  | -0.86 |  |  | -0.06 | -1.17 |  | -0.93 |  |  | Pavilion, ° |  | -0.06 |  |  |  |  |  |  | EX |  | -0.53 |  | EX |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -1.20 |  |  | -0.68 |  |  |  |  | -1.32 | -0.15 |  |  |  | -1.35 |  |  | -1.25 | -1.34 |  | -1.05 |  |  | Pavilion, notch. |  | 0.0, Negligible |  |  |  |  |  |  |  |  | 0.1 |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Pavilion painting |  |  |  |  | 0.22 |  |  | -0.20 |  |  |  |  | -0.14 | 0.34 |  |  |  | -0.39 |  |  | 0.48 | -0.53 |  | 0.23 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | -0.22 |  |  | -0.01 |  |  |  |  | -0.24 | 0.17 |  |  |  | -0.37 |  |  | -0.18 | 0.05 |  | -0.18 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Appraiser title |  |  |  |  | GIA_PCTG_StarCul |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall cut quality |  |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Symmetry appraiser title |  |  |  |  | Internal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Overall symmetry quality |  |  |  |  | VG |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle center |  |  |  |  |  |  | Culet center |  |  |  |  |  |  |  |  |  | Тable center |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |  |  |  |  | Offset by table axis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Culet |  |  |  | 0.42 ± 0.22, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.024 ± 0.013, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fluorescence |  |  |  |  |  |  |  |  |  |  |  |  | Girdle-Table |  |  |  | 0.43 ± 0.20, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.025 ± 0.011, mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  | Table-Culet |  |  |  | 0.81 ± 0.24, % |  |  |  |  |  |  |  |  |  |  |  |  | 0.047 ± 0.014, mm |  |  |  |  |  |  |  |  |  | Girdle to table-culet line offset |  |  |  |  |  |  |  | 0.24 %, 0.014 mm |  |  |  |  |  |