| # DIAMCALC STANDARD REPORT |  | # Polished Brilliant |
| --- | --- | --- |
| ## General information |  |  |
| Model | Sample Helium Brilliant |  |
| Expert name | Sample Expert Name |  |
| Report date | 06.09.2006 |  |
| Real weight, ct | 0.37 |  |
| Calculated weight, ct | 0.37, 0.3764 |  |
| Total height | 2.722 mm, 56.96 % |  |
| Total height quality | N/A |  |
| Appraiser title | AGS_2005 |  |
| Overall cut quality | 3 |  |
| Overall symmetry quality | PR |  |

## Main parameters

| Parameter |  | Avg | Min | Max | Dev | Cut | Sym |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Diameter | mm | 4.778 | 4.765 | 4.792 | 0.57 % | N/A | EX |
| Crown angle | ° | 32.25 | 31.11 | 32.55 | 1.44 | N/A | VG |
| Crown height | % | 11.38 | 10.61 | 12.35 | 1.75 | N/A | VG |
| Pavilion angle | ° | 40.68 | 39.68 | 41.53 | 1.86 | N/A | VG |
| Pavilion depth | % | 42.72 | 41.72 | 43.77 | 2.05 | N/A | GD |
| Lower girdle facets angle | ° | 41.57 | 40.59 | 42.49 | 1.90 | - | VG |
| Upper girdle facets angle | ° | 39.95 | 39.01 | 41.04 | 2.03 | - | GD |
| Star facets angle | ° | 18.74 | 17.50 | 19.77 | 2.27 | - | GD |
| Star : Upper ratio | % | 58.29 : 41.71 | 53.81 : 46.19 | 62.79: 37.21 | 8.98 | - | PR |
| Table | % | 64.03 | 63.82 | 64.12 | 0.29 | N/A | EX |
| Culet | % | 0.57 | 0.39 | 0.68 | 0.28 | 0 | EX |
| Twist | ° | 1.49 | 0.17 | 3.62 | 3.45 | - | VG |
| Girdle thickness: Bezel | % | 2.84 | 2.41 | 3.40 | 0.98 | 0 | EX |
| Girdle thickness: Bone | % | 3.31 | 3.02 | 3.71 | 0.69 |  | EX |
| Girdle thickness: Valley | % | 1.55 | 1.22 | 1.98 | 0.75 | 0 | EX |

|  | C-Height | P-Depth | Table | Culet | G-Bezel | G-Bone | G-Value |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Average value, mm | 0.544 | 2.041 | 3.059 | 0.027 | 0.136 | 0.158 | 0.074 |