| # HELIUM 8-FACETS REPORT |  |  | # Polished Brilliant |
| --- | --- | --- | --- |
| ## General information |  |  |  |
| Model | Simple |  |  |
| Expert name | Makoed A.G. |  |  |
| Report date | 19.02.2007 |  |  |
| Real weight, ct |  |  |  |
| Calculated weight, ct | 0.54, 0.5484 |  |  |
| Appraiser title | GIA_PCTG_StarCul |  |  |
| Overall cut quality | G |  |  |
| Symmetry appraiser title | Internal |  |  |
| Overall symmetry quality | GD |  |  |

## Main parameters

| Parameter |  | Avg | Min | Max | Dev | Cut | Sym |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Diameter | mm | 5.287 | 5.277 | 5.296 | 0.36 % | E | EX |
| Crown angle | ° | 34.02 | 33.45 | 34.23 | 0.78 | Grading | VG |
| Crown height | % | 15.38 | 15.06 | 15.68 | 0.62 | E | EX |
| Crown height | mm | 0.813 | 0.796 | 0.829 | 0.033 |  |  |
| Pavilion angle | ° | 40.56 | 40.44 | 40.66 | 0.21 | Grading | EX |
| Pavilion depth | % | 42.46 | 41.89 | 42.83 | 0.94 | N/A | VG |
| Pavilion depth | mm | 2.245 | 2.215 | 2.264 | 0.050 |  |  |
| Upper girdle facets angle | ° | 39.50 | 38.20 | 40.74 | 2.54 |  | GD |
| Star facets angle | ° | 21.96 | 21.31 | 22.26 | 0.95 |  | EX |
| Star : Upper ratio | % | 49.52 : 50.48 | 47.88 : 52.12 | 50.88: 49.12 | 3.00 | E | VG |
| Lower girdle facets angle | ° | 41.69 | 41.50 | 42.35 | 0.85 |  | EX |
| Total height | % | 60.97 |  |  |  | E |  |
| Total height | mm | 3.223 |  |  |  |  |  |
| Table | % | 54.40 | 53.99 | 54.72 | 0.73 | Grading | EX |
| Table | mm | 2.876 | 2.854 | 2.893 | 0.039 |  |  |
| Culet | % | 2.44 | 2.09 | 2.90 | 0.81 | G | EX |
| Culet | mm | 0.129 | 0.110 | 0.153 | 0.043 |  |  |
| Twist | ° | 0.71 | 0.05 | 1.73 | 1.68 |  | VG |
| Girdle thickness: Bezel | % | 3.11 | 2.78 | 3.35 | 0.57 | E | EX |
| Girdle thickness: Bezel | mm | 0.164 | 0.147 | 0.177 | 0.030 |  |  |
| Girdle thickness: Bone | % | 3.33 | 2.98 | 3.76 | 0.78 |  | VG |
| Girdle thickness: Bone | mm | 0.176 | 0.157 | 0.199 | 0.041 |  |  |
| Girdle thickness: Valley | % | 1.68 | 1.26 | 1.99 | 0.74 | E | EX |
| Girdle thickness: Valley | mm | 0.089 | 0.066 | 0.105 | 0.039 |  |  |

## Detailed parameters

| Parameter |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Diameter | mm | 5.281 | 5.296 | 5.288 | 5.293 |  |  |  |  |
| Crown angle | ° | 34.05 | 34.12 | 34.14 | 33.45 | 34.06 | 34.08 | 34.23 | 34.05 |
| Crown height | % | 15.68 | 15.64 | 15.41 | 15.09 | 15.06 | 15.16 | 15.35 | 15.67 |
| Crown height | mm | 0.829 | 0.827 | 0.815 | 0.798 | 0.796 | 0.802 | 0.811 | 0.828 |
| Crown azimuth | ° | 0.3 | 44.4 | 90.1 | 136.1 | 179.5 | 225.6 | 269.8 | 315.9 |
| Pavilion angle | ° | 40.44 | 40.53 | 40.55 | 40.55 | 40.55 | 40.64 | 40.60 | 40.66 |
| Pavilion depth | % | 41.89 | 42.30 | 42.49 | 42.54 | 42.68 | 42.83 | 42.51 | 42.45 |
| Pavilion depth | mm | 2.215 | 2.236 | 2.246 | 2.249 | 2.256 | 2.264 | 2.247 | 2.244 |
| Pavilion azimuth | ° | 0.0 | 45.4 | 90.1 | 135.7 | 180.1 | 224.7 | 269.2 | 314.2 |
| Upper girdle facets angle | ° | 38.68 | 39.37 | 38.20 | 38.21 | 40.00 | 39.97 | 39.07 | 39.53 |
|  |  | 39.25 | 39.27 | 39.98 | 39.72 | 40.55 | 40.74 | 39.88 | 39.63 |
| Star facets angle | ° | 22.10 | 21.68 | 21.31 | 22.03 | 22.16 | 22.04 | 22.26 | 22.09 |
| Star : Upper ratio | % | 47.88 : 52.12 | 48.63 : 51.37 | 50.26 : 49.74 | 50.29 : 49.71 | 49.93 : 50.07 | 48.73 : 51.27 | 50.88 : 49.12 | 49.51 : 50.49 |
| Lower girdle facets angle | ° | 41.52 | 41.54 | 42.35 | 42.19 | 41.63 | 41.55 | 41.59 | 41.54 |
|  |  | 41.66 | 41.69 | 41.69 | 41.62 | 41.63 | 41.76 | 41.63 | 41.50 |
| Table | % | 54.22 | 54.72 | 54.66 | 53.99 |  |  |  |  |
| Table | mm | 2.867 | 2.893 | 2.890 | 2.854 |  |  |  |  |
| Twist | ° | 0.33 | 1.07 | 0.05 | 0.37 | 0.63 | 0.82 | 0.66 | 1.73 |
| Girdle Bezel | % | 3.32 | 2.96 | 3.07 | 3.35 | 3.24 | 2.98 | 3.15 | 2.78 |
| Girdle Bezel | mm | 0.175 | 0.156 | 0.162 | 0.177 | 0.171 | 0.157 | 0.167 | 0.147 |
| Girdle Bone | % | 3.76 | 2.98 | 3.29 | 3.39 | 3.49 | 3.27 | 3.10 | 3.36 |
| Girdle Bone | mm | 0.199 | 0.157 | 0.174 | 0.179 | 0.184 | 0.173 | 0.164 | 0.178 |
| Girdle Valley | % | 1.99 | 1.77 | 1.26 | 1.66 | 1.53 | 1.67 | 1.84 | 1.89 |
|  |  | 1.73 | 1.64 | 1.53 | 1.82 | 1.65 | 1.37 | 1.57 | 1.93 |
| Girdle Valley | mm | 0.105 | 0.094 | 0.066 | 0.088 | 0.081 | 0.089 | 0.097 | 0.100 |
|  |  | 0.092 | 0.087 | 0.081 | 0.096 | 0.087 | 0.072 | 0.083 | 0.102 |