| # HELIUM FULL REPORT |  | # Semi-polished Princess |  |
| --- | --- | --- | --- |
| ## General information |  |  |  |
| Model | Simple |  |  |
| Expert name | Makoed A.G. |  |  |
| Report date | 29.11.2006 |  |  |
| Real weight, ct |  |  |  |
| Calculated weight, ct | 0.56, 0.5600 |  |  |
| Spread | -0.06 ct, -11.21 % |  |  |

## Main parameters

| Parameter |  | Avg | Min | Max | Dev |
| --- | --- | --- | --- | --- | --- |
| Width, length | mm |  | 4.523 | 4.612 | Ratio: 1.020 |
| Corner width | % | 142.46 | 141.61 | 143.31 | 1.70 |
| Corner width | mm | 6.444 | 6.406 | 6.482 | 0.077 |
| Corner width ratio |  | 1.012 |  |  |  |
| Crown height: Side | % | 8.78 | 8.39 | 9.06 | 0.67 |
| Crown height: Side | mm | 0.397 | 0.379 | 0.410 | 0.030 |
| Crown height: Corner | % | 8.83 | 8.55 | 9.18 | 0.63 |
| Crown height: Corner | mm | 0.399 | 0.387 | 0.415 | 0.029 |
| Pavilion height: Side | % | 57.22 | 56.04 | 57.79 | 1.75 |
| Pavilion height: Side | mm | 2.588 | 2.535 | 2.614 | 0.079 |
| Pavilion height: Corner | % | 57.61 | 56.31 | 59.07 | 2.76 |
| Pavilion height: Corner | mm | 2.606 | 2.547 | 2.672 | 0.125 |
| Total height | % | 69.21 |  |  |  |
| Total height | mm | 3.131 |  |  |  |
| Table: Side | % | 80.69 | 80.47 | 80.92 | 0.45 |
| Table: Side | mm | 3.686 | 3.640 | 3.732 | 0.092 |
| Table: Corner w.r.t. Corner | % | 80.72 | 80.42 | 81.02 | 0.60 |
| Table: Corner w.r.t. Width | % | 114.99 | 114.74 | 115.25 | 0.52 |
| Table: Corner | mm | 5.202 | 5.190 | 5.213 | 0.023 |
| Culet | % | 0.34 | 0.24 | 0.39 | 0.15 |
| Culet | mm | 0.016 | 0.011 | 0.018 | 0.007 |
| Girdle thickness: Side | % | 3.21 | 2.64 | 4.11 | 1.47 |
| Girdle thickness: Side | mm | 0.145 | 0.119 | 0.186 | 0.067 |
| Girdle thickness: Corner | % | 2.77 | 1.59 | 4.15 | 2.56 |
| Girdle thickness: Corner | mm | 0.126 | 0.072 | 0.188 | 0.116 |

## Detailed parameters

| Parameter |  | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- | --- |
| Corner width | % | 143.31 | 141.61 |  |  |
| Corner width | mm | 6.482 | 6.406 |  |  |
| Crown height: Side | % | 8.39 | 8.80 | 9.06 | 8.86 |
| Crown height: Side | mm | 0.379 | 0.398 | 0.410 | 0.401 |
| Crown height: Corner | % | 8.75 | 8.83 | 9.18 | 8.55 |
| Crown height: Corner | mm | 0.396 | 0.399 | 0.415 | 0.387 |
| Pavilion height: Side | % | 57.79 | 57.35 | 56.04 | 57.71 |
| Pavilion height: Side | mm | 2.614 | 2.594 | 2.535 | 2.611 |
| Pavilion height: Corner | % | 56.31 | 58.35 | 56.71 | 59.07 |
| Pavilion height: Corner | mm | 2.547 | 2.639 | 2.565 | 2.672 |
| Table: Side | % | 80.47 | 80.92 |  |  |
| Table: Side | mm | 3.640 | 3.732 |  |  |
| Table: Corner w.r.t. Corner | % | 80.42 | 81.02 |  |  |
| Table: Corner w.r.t. Width | % | 115.25 | 114.74 |  |  |
| Table: Corner | mm | 5.213 | 5.190 |  |  |
| Girdle thickness: Side | % | 3.03 | 3.06 | 4.11 | 2.64 |
| Girdle thickness: Corner | % | 4.15 | 2.04 | 3.32 | 1.59 |
| Girdle thickness: Side | mm | 0.137 | 0.139 | 0.186 | 0.119 |
| Girdle thickness: Corner | mm | 0.188 | 0.092 | 0.150 | 0.072 |

| Offset |  | Distance | Width wise | Length wise |
| --- | --- | --- | --- | --- |
| Culet-Table offset by table axis | % | 1.06 ± 0.29 | 0.09 | 1.06 |
| Culet-Table offset by table axis | mm | 0.048 ± 0.013 | 0.004 | 0.048 |
| Girdle-Culet offset by table axis | % | 1.21 ± 0.28 | 0.26 | 1.19 |
| Girdle-Culet offset by table axis | mm | 0.055 ± 0.013 | 0.012 | 0.054 |
| Girdle-Table offset by table axis | % | 0.22 ± 0.24 | 0.17 | 0.13 |
| Girdle-Table offset by table axis | mm | 0.010 ± 0.011 | 0.008 | 0.006 |
| Girdle to table-culet line offset | % | 0.35 |  |  |
| Girdle to table-culet line offset | mm | 0.016 |  |  |

| Culet shift ratio by width & length |  |  |
| --- | --- | --- |
| Width | 4.523 mm, 100% |  |
| Width-wise culet shift ratio | 2.277 mm, 50.33 % | 2.247 mm, 49.67 % |
| Length | 4.612 mm, 100% |  |
| Lengh-wise culet shift ratio | 2.271 mm, 49.24 % | 2.381 mm, 51.62 % |

| Culet shift ratio by main diameter |  |  |
| --- | --- | --- |
| Main diameter (width) | 4.523 mm, 100% |  |
| Width-wise culet shift ratio | 2.277 mm, 50.33 % | 2.247 mm, 49.67 % |
| Lengh-wise culet shift ratio | 2.271 mm, 50.21 % | 2.381 mm, 52.63 % |

## Crown and pavilion views of the diamond with indication of the diameter minimum and maximum

| Invisible edges are hidden |  |  |
| --- | --- | --- |
| Invisible edges are drawn taking refraction into account |  |  |

## Plots

| Girdle thickness plot |  |  |
| --- | --- | --- |
| Diameter variation plot |  |  |

## Facets' azimuth and slope angles

| Pavilion and crown views of the diamond with indication of facets' azimuth angles |  |
| --- | --- |
| Pavilion and crown views of the diamond with indication of facets' slope angles |  |

## Facets' heights

| Pavilion and crown views of the diamond with indication of facets' heights (mm) |  |
| --- | --- |
| Pavilion and crown views of the diamond with indication of facets' heights (%) |  |

## Additional illustrations

| Pavilion and crown views of the diamond with indication of invisible edges without refraction |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |

|  | Girdle center |  | Culet center |  | Table center |
| --- | --- | --- | --- | --- | --- |